## Slide 1: Electrospray from Magneto-electrostatic Instabilities
Lyon B. King, Kurt Terhune, Brandon Jackson, Amanda O’Toole, Stephan den Hartog, Nathan Ford
Juan Fernandez de la Mora, Aaron Madden, Javier Cubas
Deborah Levin, Neil Mehta
Brian Hawkett, Nirmesh Jain
December 9, 2015

## Slide 4
Magnetic field:
Gas density:
r

## Slide 5: Electrospray: plasma in a bottle

## Slide 6
Zeleny, J., "The electrical discharge from liquid points, and a hydrostatic method of measuring the electric intensity at their surfaces," Physical Review, 3(2), 1914, 69-91.
Jean-Antoine Nollet – 1750:
“a person, electrified by connection to a high-voltage generator, would not bleed normally if he were to cut himself; blood would spray from the wound.”

## Slide 7
Neutral Fluid
Surface tension is balanced by fluid pressure

## Slide 8
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
- - - - - - - - - - - - - - - -
+ + + + + + + + + + + +
E
E
Neutral Fluid
Electrohydrodynamic
Stress
Surface tension is balanced by fluid pressure

## Slide 9
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
- - - - - - - - - - - - - - - -
+ + + + + + + + + + + +
E
E
N N N N N N N N N N
S S S S S S S S S S S S S
H
H
Neutral Fluid
Electrohydrodynamic
Stress
Ferrohydrodynamic
Stress
Surface tension is balanced by fluid pressure

## Slide 10
500 microns
Magnet
Explore new fluid mechanics of combined ferro- and electrohydrodynamic spray emission
Increasing E

## Slide 11: New material: Ionic liquid ferrofluid
6 Jain, N. et at., Stable and Water-Tolerant Ionic Liquid Ferrofluid. Applied Materials and Interfaces 2011 (3): p. 662-667
7 Huang, W. and Wang, X., Stuy on the properties and stability of ionic liquid-based ferrofluids. Colloid Polym Sci, 2012 290: p. 1695-1702
11
Jain et al 6 :
EAN with Fe2O3
EMIM-Ac with Fe2O3
EMIM-SCN with Fe2O3
Huang and Wang 7 :
EMIM-ethylsulphate with CoFe2O4
EAN with Sirtex nanoparticles
2011
2012
2013
Present
EMIM-NtF2
Sulfolane + EAN
Triglyme
Glycerol
(all with Sirtex MNPs)
Collaboration between and

## Slide 12: How to make a Ferrofluid
T ~ Room Temp
No applied field
Mnet = 0
T ~ Room Temp
Applied Field
Mnet > 0
T > Curie Temp
Applied Field
Mnet~ 0
H
Melting a Ferromagnetic
Substance Doesn’t Work:
H
T > Tlliquid
Mnet = 0
H

## Slide 13: How to make a Ferrofluid
T ~ Room Temp
No applied field
Mnet = 0
T ~ Room Temp
Applied Field
Mnet > 0
T > Curie Temp
Applied Field
Mnet~ 0
H
Melting a Ferromagnetic
Substance Doesn’t Work:
H
T > Tlliquid
Mnet = 0
H
H
Mnet > 0
A Ferrofluid is a Superparamagnetic Colloid:
Solid-state ferromagnetic particles
small enough to contain only
a single magnetic domain (10s of nm)
Carrier liquid
M (A/m)
H (A/m)
Because the particles are free to rotate
The M-H curve does not display hysteresis

## Slide 14
Magnetohydrodynamics
Electrohydrodynamics
Ferrohydrodynamics
Ionic liquid ferrofluid: a truly magnetized plasma
Lorentz Force
Coulomb Force
Kelvin Force
Momentum:
Quasi-static Maxwell:
Young-Laplace:
Notes: One interesting effect is a spray instability that we can induce with E and B.

## Slide 15: Determine Critical Fields for Spray Onset
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
N
S
+
+
+
+
+
+
+
+
+
+
COMSOL Microfluidics with electromagnetic stress
Two-phase transient flow with moving mesh (ALE)
Experimentally determined M-H characteristic for fluid
Experimentally determined fluid-solid contact angle
Numerical Simulation of Ferrofluid Droplet
Fluid interface
geometry
Electric
Stress
Magnetic
Stress
Capillary
Stress
Hydrostatic
Pressure
Fluid meniscus geometry is non-linear equilibrium
Magnet

## Slide 16: Numerical Model Validation
Transient Droplet Dynamics
Silhouette Image
Model Validation
Collimated Backlight Imager
Droplet on Flat Plate in Helmholtz Coil
Ferrotec EFH-1 on
Brass slide

## Slide 17: Interfacial Magneto-electrostatic Stress
Experimental Silhouette Images
Numerical Simulation

## Slide 18
Zeleny, J., "The electrical discharge from liquid points, and a hydrostatic method of measuring the electric intensity at their surfaces," Physical Review, 3(2), 1914, 69-91.
Compare with Established Theory: Capillary Electrospray

## Slide 19: Capillary Studies: Motivation and Approach
Spray current
Flow rate
Conductivity
Permittivity
Surface tension
Existing Electrospray Theory
(over 400 citations):
Fernandez de la Mora, J., and Loscertales, I.G., “The current emitted by highly conducting Taylor cones,” J. Fluid Mech. 260, 155-184, 1994.

## Slide 20: Capillary Studies: Motivation and Approach
Ferrofluid base | Sulfolane + 0.1% EAN | Sulfolane + 1% EAN | Sulfolane + 10% EAN | EMIM-NTf2
Conductivity (S/m) | 0.012 | 0.033 | 0.324 | 0.57
Ferrofluids synthesized by University of Sydney Key Centre for Polymers and Colloids (Hawkett and Jain) by stabilizing ~ 50-nm-diameter maghemite particles supplied by Sirtex Medical, Ltd.
Sprayed in atmosphere
Sprayed in vacuum
Spray current
Flow rate
Conductivity
Permittivity
Surface tension
Existing Electrospray Theory
(over 400 citations):
Fernandez de la Mora, J., and Loscertales, I.G., “The current emitted by highly conducting Taylor cones,” J. Fluid Mech. 260, 155-184, 1994.

## Slide 21: Capillary Spray Results
Increasing B
Decreasing B
Spray current
Flow rate
Conductivity
Permittivity
Surface tension
Existing Electrospray Theory
(over 400 citations):
Fernandez de la Mora, J., and Loscertales, I.G., “The current emitted by highly conducting Taylor cones,” J. Fluid Mech. 260, 155-184, 1994.
Pure EMIM-NTf2
EMIM-NTf2 Ferrofluid
Magnetic effects increase current by ~ 40%

## Slide 22: Capillary Spray Results
Existing Electrospray Theory:
Current still scales with square root of flow rate, but magnetic field increases the magnitude

## Slide 23: Magnetic Stress Extends Spray Stability Range
Lower stable flow rates will enable smaller droplet sizes
Magnetic Field Damps Oscillations
EMIM-NTf2
Ferrofluid
Sulfolane
Ferrofluid
Sulfolane
Ferrofluid
Sulfolane
Ferrofluid
B = 0 G
B = 295 G

## Slide 24: Theoretical Model of Jet Stability
Stable
Unstable
Dispersion Relation for Surface Waves
Theoretical model of fluid cylinder stability against surface perturbation
Liquid is electrically conducting ferrofluid
Axial magnetic field has a stabilizing effect against surface perturbations
Dipole alignment augments surface tension
m=0 mode
H = 300 G
E = 200 V/mm

## Slide 25
Gravitational
Surface Tension
Magnetic
Notes: Single mountain does not minimize energy.

## Slide 26
Self-assembling Array of Electrospray Emitters Fabricated from the Propellant Itself
Emitter array fabricated in silicon
Rosensweig instability in ionic liquid ferrofluid

## Slide 27
5mm
Aluminum Fluid Holder
Extraction Electrode and Current Collector
Rosensweig Instability in Ionic liquid with Sirtex nanoparticles
E
B

## Slide 30
Permanent Magnet
M
M

## Slide 31: Where we’re going…