## Slide 1
DRY ETCHING OF Si3N4 USING REMOTE PLASMA SOURCES SUSTAINED
IN NF3 MIXTURES*
Shuo Huang and Mark J. Kushner
Department of Electrical Engineering and Computer Science,
University of Michigan, Ann Arbor, MI 48109
(shuoh@umich.edu, mjkush@umich.edu)
The 6th Annual MIPSE Graduate Student Symposium
Ann Arbor, Michigan
October 7, 2015
Work supported by Samsung Electronics, DOE Office of Fusion Energy Science and National Science Foundation.
Notes: 1
1

## Slide 2
University of Michigan
Institute for Plasma Science & Engr.
AGENDA
Remote NF3 sources
NF3 electron impact cross sections
Gas phase and surface reaction mechanisms
Description of the model
Plasma properties and etch rates
  Continuous wave scenarios
  Pulsed power scenarios
  Different gas mixtures
Concluding Remarks
Notes: 2
2

## Slide 3
University of Michigan
Institute for Plasma Science & Engr.
REMOTE PLASMA SOURCES
Remote plasma sources (RPS) for microelectronics fabrication:
  Produce dominantly neutral fluxes of radicals for etching, cleaning, surface passivation
  Decrease damage by charging and energetic ion bombardment.
[1] Kastenmeier et al., JVSTA 16, 2047 (1998).
Separate plasma production, transport and processing regions.
  Small effect of E-field on particle transport near wafer.
  Particle transport dominated by convective flow and diffusion.
RPS use distance, grids or other discriminating barriers to limit exposure to plasma.
Schematic of RPS.[1]
Notes: 3
3

## Slide 4
University of Michigan
Institute for Plasma Science & Engr.
In NF3 containing mixtures, F efficiently produced by dissociative processes:
e + NFn (n=1-3)  NFn-1 + F-
  e + NFn (n=1-3)  NFn-1 + F + e.
F-containing plasmas used for etching Si-containing materials.
  SiFm-1(s) + F(gas)  SiFm(ads, m=1-3)
  SiF3(s) + F(gas)  SiF4(gas).
Pure NF3 limits variety of reactive fluxes to F, NFn. Additives (NF3/O2, NF3/H2) increase variety of reactive species to optimize process.
NO produced in NF3/O2 mixtures aids removal of N from Si3N4.[2]
  N(surface) + NO(gas)  N2(gas) + O(surface)
   N2O(gas).
NF3 GAS MIXTURES
[2] Kastenmeier et al., JVSTA 19, 25 (2001).

## Slide 5
University of Michigan
Institute for Plasma Science & Engr.
Cross sections for NF3 based on work of V. Lisovskiy et al.[3]
ELECTRON IMPACT NF3 CROSS SECTIONS
[3] V. Lisovskiy et al., J. Phys. D 47, 115203 (2014).
Cross sections for NF3 calculated using R-matrix method.
Differences in dissociative electron attachment at low energy does impact predictions of RPS efficiency.

## Slide 6
University of Michigan
Institute for Plasma Science & Engr.
N, N2
NF
NF3
NF2
FO
NO, NO2
F, F2
O, O2
O, O2, O3
e, O, NO, M
N,
N2,
FNO
e,
N,
NO,
NO2,
M
F,
FO,
M
F2
O
O, FO, NO, NF2, M
O, F, NO
e,
NF,
M
e
e, N,
NF, M
e,
N,
M
e,
M
e, N
e, N,
NF, M
F2, NF2
e, N, NF2, O, M
NF3
FNO
O, FO, NO2
O
F2
NF2
M represents 3rd body.
  Electron modified enthalpy (gas heating).
NF2
O
NO
O3
O2
e,
N,
NO,
M
N
REACTION MECHANISM: NF3/O2
Notes: 6
6

## Slide 7
University of Michigan
Institute for Plasma Science & Engr.
PRIMARY SURFACE MECHANISM FOR Si3N4 ETCHING
In RPS systems, there are negligible fluxes of ions (with above thermal energies) to substrate.
Mechanism is purely neutral driven.
Si in Si3N4 is removed by a sequence of F-passivation steps.
        SiN(s) + F(g)  SiNF(s)
        SiNF(s) + F(g)  SiNF2(s)
        SiNF2(s) + F(g)  SiNF3(s)
        SiNF3(s) + F(g)  SiF4(g) + N(s)
NO aids removal of N surface sites through 2 channels.
        N(s) + NO(g)  N2(g) + O(s)
        O(s) + NO(g)  NO2(g) +SiN(s)
        O(s) + O(g)  O2(g) + SiN (s)
        O(s) + O(s)  O2(g) + SiN(s)
        N(s) + NO(g)  N2O(g) + SiN(s)

## Slide 8
Plasma Chemistry
Monte Carlo Simulation
Surface
Kinetics
Module
Hybrid Plasma Equipment Model – modular simulator that combines fluid and kinetic approaches.
Surface Kinetics Module (SKM) – a surface site balance model addressing etching, deposition and passivation of surfaces.
Fluid-Kinetics Poisson Module (FKPM): Heavy particle and electron continuity, momentum, energy and Poisson’s equations.
Electron, Ion Cross Section Database
DESCRIPTION OF HPEM
EETM
FKPM
University of Michigan
Institute for Plasma Science & Engr.

## Slide 9
University of Michigan
Institute for Plasma Science & Engr.
Inductively coupled RPS.
Mini-showerheads to isolate ions.
Ar/NF3/O2, 50 mTorr, 3000 sccm.
Flow distance: 12 cm.
CW cases:
  Power: 100 – 800 W.
  Ar/NF3/O2=(100-2X)/X/X: X=5-20.
Pulsed cases:
  PRF=20, 50, 100 kHz.
  Duty cycle=30, 50%
  Pave = 300 W.
REMOTE PLASMA SOURCE

## Slide 10
University of Michigan
Institute for Plasma Science & Engr.
ne, Te : 300 W (CW)
Electron confinement results from highly attaching chemistry and grid of shower-head. (D = 0.08 cm at showerhead.)
[e]: 4  1011 cm-3, Te = 4.5 eV
MIN
MAX

## Slide 11
University of Michigan
Institute for Plasma Science & Engr.
IONIZATION SOURCE – ION-ION PLASMA (CW)
Ions are largely confined to source region, however a weak ion-ion plasma persists to lower chamber.
Ion-ion plasma in lower chamber: [F-]  [NO+] + [O2+]  108 cm-3.
Negligible flux of ions to wafer surface.
MIN
MAX

## Slide 12
University of Michigan
Institute for Plasma Science & Engr.
RADICAL GENERATION – 300 W (CW)
F efficiently produced with 50% dissociation of NF3.
[NO] produced by endothermic processes aided by gas heating:
N2 + O2  NO + NO N2 + O  N + NO.
Gas temperature in RPS  750 K.
MIN
MAX

## Slide 13
University of Michigan
Institute for Plasma Science & Engr.
ETCH RATE – 300 W (CW)
Si surface sites etched by F, forming SiF4 and exposing N sites.
N sites etched by NO aided processes:
        (I) N(s) + NO(g)  N2(g) + O(s)
        O(s) + NO(g)  NO2(g) + SiN(s)
        O(s) + O(g)  O2 + SiN(s)
        O(s) + O(s)  O2(g) + SiN(s)
        (II) N(s) + NO  N2O + SiN(s)
For these conditions, limiting factor for etch rate is ratio of NO/F fluxes.
Other possible channel to remove N sites: N(s) + N(g)  N2(g).

## Slide 14
University of Michigan
Institute for Plasma Science & Engr.
FLUXES, ETCH RATE vs. POWER (CW)
 F Flux
F flux increases linearly with power until saturating when NF3 dissociation becomes significant.
NO flux increases non-linearly with power due to 2-step and/or endothermic formation mechanism, requiring higher radical densities and gas temperature. F/NO ratio decreases with power.
Result is threshold power for significant etching based on availability of NO.
 NO Flux
 Etch Rate

## Slide 15
University of Michigan
Institute for Plasma Science & Engr.
SURFACE COVERAGE vs. POWER (CW)
Fractional Si surface sites
Fractional N surface sites
Initial condition: pristine SiN sites containing Si and N "subs-sites".
Si "sub-sites" in SiN almost completely etched by F atoms leaving N "sub-sites". Full etching is rate limited by removal of N sub-sites.
Etching of N sites depends on NO density: higher NO flux leads to removal of N sites and re-exposure of SiN sites.

## Slide 16
University of Michigan
Institute for Plasma Science & Engr.
FLUXES, ETCH RATE vs. GAS MIXTURE (CW)
Similar trends when varying gas mixture.
F atom flux increases with NF3 fraction however, NO flux nearly constant for constant power – due, in part, to endothermic origin and dependence on gas temperature.
Result is limited dependence of etch rate on mixture as long as NO fluxes are critically large.
 F Flux
 NO Flux
 Etch Rate

## Slide 17
University of Michigan
Institute for Plasma Science & Engr.
Use of pulse power provides a means for modulating electron energy distribution (EED), and so control radical generation.
Pulsing enables both plasma properties and etch properties to be controlled beyond what may be possible with CW excitation.
Pulse repetition frequency: 20, 50, 100 kHz.
Duty Cycle = 30, 50%.
Average power: 300 W.
PULSED POWER

## Slide 18
University of Michigan
Institute for Plasma Science & Engr.
CHARGED SPECIES – 20 kHz, 30% DUTY CYCLE
With a fast rising pulse, over-shoot in E/N and Te above cw values enable more efficient excitation.
Source and loss for e’s balance over 1 pulse period:
  Pulse-on: ionization,
  Pulse-off: diffusion, attachment, and recombination.
Customizable rate coefficients compared to CW operation.

## Slide 19
University of Michigan
Institute for Plasma Science & Engr.
[e], [NO+] – 20 kHz, 30% DC
Terminal positive ion is NO+ due to favorable charge exchange.
As density of NO increases flowing downstream, NO+ density increases.
MIN
MAX
Animation Slide

## Slide 20
University of Michigan
Institute for Plasma Science & Engr.
NO DENSITY AND FLUX – 20 kHz, 30% DC
Since radical lifetime and residence time are longer than pulse period, little modulation in NO densities and fluxes.
Lower PRF could be leveraged to sequence fluxes to substrate.
MIN
MAX
Animation Slide

## Slide 21
University of Michigan
Institute for Plasma Science & Engr.
ETCH RATE vs. PRF, DUTY CYCLE
PRF: 20 – 100 kHz
Duty cycle: 30 – 50% DC
Etch rate sensitive to PRF and duty cycle for same average power due to production rates of NO.
With increasing PRF, average gas temperature increases.
With decreasing DC, Tgas during pulse increases.

## Slide 22
University of Michigan
Institute for Plasma Science & Engr.
CONCLUDING REMARKS
RPS has been modeled using ICP operation of HPEM (2-D).
Electron-impact NF3 cross sections has been calculated using ab initio R-matrix method.
Etch rates correlate with NO flux which produces non-linear scaling with power but weak dependence on mixture.
Etch rate increases with increased PRF and decreased duty cycle:
  Over-shoot in E/N and Te above cw values enable more efficient excitation and gas heating.
  NO density modulated through gas heating.
Notes: 22
22