## Slide 1
ONSET OF SILICON NANOPARTICLE CRYSTALLINITY IN NONTHERMAL PLASMAS
Yifan Gui1, Jordyn Polito2 and Mark J Kushner3
* Work supported by Army Research Office MURI Grant W911NF-18-1-0240, the National Science Foundation (PHY-2009219), and the Department of Energy Office of Fusion Energy Science (No.DE-SC0020232).
1Department of Nuclear Engineering and Radiological Sciences
2Department of Chemical Engineering
3Department of Electrical Engineering and Computer Science
University of Michigan, Ann Arbor, MI 48109 USA
evangyf@umich.edu, jopolito@umich.edu, mjkush@umich.edu
http://uigelz.eecs.umich.edu
MIPSE Symposium 2024
Notes: 1

## Slide 2
R. Anthony et al. Phy. Review B 80, 115407 (2009).
X. D. Pi et al. Nanotechnology 19, 245603 (2008).
CRYSTALLINE NANOPARTICLES
University of Michigan
Institute for Plasma Science & Engr.
Controlling size uniformity, purity and crystallinity of NPs is crucial.
Photoluminescence quantum yield (PLQY) increases from 2 to 40% as Si NP crystallizes. [1]
Crystalline NPs can be produced through high temperature annealing.
Capacitively coupled plasmas (CCPs) vs. inductively coupled plasmas (ICPs).
[1] R. Anthony et al. Phys. Review B 80, 115407 (2009).
Notes: 2

## Slide 3
MODELING PLATFORMS
University of Michigan
Institute for Plasma Science & Engr.
Modular HPEM to address physical processes in low-temperature plasmas using fluid and kinetic approaches.
DTS workflow:
  Temperature, densities, neutral/ion momenta, and electric fields from HPEM
  Initialize NPs; Compute growth, charging, temperature and the forces acting on the NPs
  Generates a 3-D trajectory for each NP
  Feed NP density and charge back to HPEM
Notes: 3
Forces on NPs:
  Electrostatic
  Gravitational
  Thermophoretic
  Ion drag
  Fluid drag
  Interparticle Coulombic interactions

## Slide 4
REACTOR GEOMETRIES
Cylindrical CCP and ICP reactors to create NP growth zone.
2 cm radius, 10 cm height.
Ar/SiH4 = 98/2, 50 sccm
1 Torr
10 W, 10 MHz
University of Michigan
Institute for Plasma Science & Engr.
Plasma Zone
CCP electrodes
Inlet
Outlet
Glass
Plasma Zone
ICP antennae
Reactor Height (cm)
Radius (cm)
Radius (cm)
CCP
ICP
Notes: 4

## Slide 5
NP HEATING
University of Michigan
Institute for Plasma Science & Engr.
  NP temperature computed based on approach of Kramer et al. [3].
[3] N. J. Kramer et al J. Phys. D: Appl. Phys. 47, 075202 (2014)
  Cooling
    Heat conduction to gas, continuously computed
    Radiative loss
  Gain
    Ion recombination (freq. from OML theory)
    Hydrogen atom and radical growth reactions.
Notes: 5

## Slide 6
NP GROWTH
University of Michigan
Institute for Plasma Science & Engr.
    SiH4 breaks into radicals by electron impact dissociation.
    These radicals stick to NPs.
    Sticking coefficients (Sc) of radicals from molecular dynamics simulations [2].
    Although unlikely, NPs can coagulate.
2 dec., [cm-3]
[2] X. Shi et al, J. Phys. D: Appl. Phys. 54, 365203 (2021)
Radius (cm)
Height (cm)
SiH4
7.8×1014
Sc=0
SiH3
7.7×1011
Sc=0.125
SiH2
8.45×1011
Sc=0.66
SiH
9.6×1010
Sc=0.945
0
2
4
6
8
10
0
1
0
1
0
1
0
1
2
ICP, 1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 6
Need to change this slide

## Slide 7
NP TRANSPORT
University of Michigan
Institute for Plasma Science & Engr.
Animation
NP Diameter
11 nm
2 nm
NP Charge
-1 q
-20 q
Top down view
t = 0 – 0.85 s
CCP, 1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
NPs initialization at nucleation sites
NPs trap in ring formation
NPs de-trap
Notes: 7
Si NPs were initialized as “seeds” with 1 nm radius between electrodes.
NPs are charged negatively due to the higher mobility of electrons.
Electrostatic forces traps the NPs near regions of maximum potential.
Thermophoresis and ion drag force pushes NPs radially outward to form ring-like structures.
NPs grow to critical size when fluid drag dominates and flow out of the reactor.

## Slide 8
NP TEMPERATURE
University of Michigan
Institute for Plasma Science & Engr.
  Stochastic ion and neutral reactions produce impulsive energy gain in NPs.
  Reactions occurring at high frequency enables TNP build-up, followed by rapid conductive cooling.
  TNP decreases with increasing NP size.
ICP, 1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 8

## Slide 9
NP CRYSTALLIZATION vs. NP SIZE
University of Michigan
Institute for Plasma Science & Engr.
  Only smaller NPs have TNP above Tc.
  Large NCs are synthesized in plasma reactors [5].
  Hypothesis: Large NCs grow epitaxially on thermally produced smaller crystalline cores.
[4] M. Hirasawa et al. Appl. Phys. Lett. 88, 093119 (2006)
[5] U. R. Kortshagen et al, Chem. Rev. 116, 11061 (2016).
  Hirasawa et al investigated NP crystallization temperature Tc vs NP size [4].
  4 nm: 773 K
  6 nm: 1073 K
  8 nm: 1173 K
  10 nm: 1273 K (Red lines)
ICP, 1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 9

## Slide 10
Tc
TNP
University of Michigan
Institute for Plasma Science & Engr.
MODELING NANOCRYSTAL FORMATION
15
[6] C. Sun and D. Xue, Curr. Opin. Chem. Eng. 1, 108 (2012).
ICP, 1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
DTS tracks the NP “exposure time”, defined as the length of time TNP > Tc (in red).
Maximum exposure time, tmax, determines the performance of CCP and ICP for NP crystallization.
tmax is the maximum time NP spends in the reactor with TNP > Tc.
Larger the tmax, more optimal the reactor configuration is for NC production.
tmax
Notes: 10
50 sccm:
σ = 0.08 nm,
Ge/Si core/shell radius = 7.6/0.1 nm

## Slide 11
CCP vs. ICP FOR NP CRYSTALLIZATION
Notes: 11

## Slide 12
CCP vs. ICP PLASMA PROPERTIES
University of Michigan
Institute for Plasma Science & Engr.
1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
ICPs have higher plasma density than CCPs.
CCPs are characterized by their plasma uniformity and higher electron temperature Te.
ICP plasma potential tends to be more localized and quiescent compared to CCPs (stronger electrostatic NP traps).
0
2
4
6
8
10
Height (cm)
0
1
2
0
1
0
1
Radius (cm)
ICP CW
CCP CW
0
2
4
6
8
10
Height (cm)
0
1
2
0
1
0
1
Radius (cm)
[e], 1.15×1010 cm-3, 2 dec.
Te, 1 – 12 eV
Plasma potential, -100 – 130 V
[e], 3.72×1011 cm-3, 2 dec.
Te, 0.5 – 3.4 eV
Plasma potential, 0 – 23 V
Notes: 12

## Slide 13
CCP
ICP
NP CRYSTALLIZATION: CCP vs. ICP
University of Michigan
Institute for Plasma Science & Engr.
TNP is higher for ICP than CCP due to the larger plasma density. (3.72×1011 vs. 1.15×1010 cm-3 )
TNP > Tc up to 4 nm NPs in ICP.
1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 13

## Slide 14
NP CRYSTALLIZATION: CCP vs. ICP
University of Michigan
Institute for Plasma Science & Engr.
CCP
ICP
tmax = 0.15 s
tmax = 0.035 s
t = 0 – 0.25 s
tmax achieved
Not crystalline
Animation Slide
ICP achieving tmax occurs sooner.
NPs are in crystallization process for shorter time in ICP.
tmax is 4 times higher for CCP than ICP.
1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 14

## Slide 15
NP CRYSTALLIZATION: CCP vs. ICP
University of Michigan
Institute for Plasma Science & Engr.
0
2
4
6
8
ICP
[SixHy ]
2.5×1012, 2 dec.
Radius (cm)
CCP
[SixHy ]
8.5×1011, 2 dec.
0
2
4
6
8
10
0
1
Height (cm)
[cm-3]
10
0
1
2
2
Growth species density in ICP is 4 times larger, faster growth rate.
NPs spend less time being “small” → less time with TNP>Tc.
Higher plasma density does not equate to more crystalline particles!
1 Torr, 10 W, 50 sccm, Ar/SiH4 98/2
Notes: 15

## Slide 16
CONTINUOUS WAVE (CW) vs. PULSED ICP FOR NP CRYSTALLIZATION
Notes: 16

## Slide 17
CW vs. PULSED ICP PLASMA PROPERTIES
University of Michigan
Institute for Plasma Science & Engr.
1 Torr, 10 W (1ms, 0.5 DC), 50 sccm, Ar/SiH4 98/2
Plasma density, temperature and potential of pulsed plasmas are higher at the onset of the pulse compared to cw.
During power-off period, ne decreases as dissociative recombination, diffusion and thermal attachment reactions begin to dominate.
Animation
Notes: 17

## Slide 18
PULSED
CW
NP CRYSTALLIZATION: CW vs. PULSED ICP
University of Michigan
Institute for Plasma Science & Engr.
10 W, 1 ms, 0.3 – 0.7 duty cycle (DC).
TNP is higher for pulsed ICP due to the larger plasma density at onset of pulse.
Pulsed ICP pushes the crystallization limit to 6 nm.
Notes: 18

## Slide 19
NP CRYSTALLIZATION: CW vs. PULSED ICP
University of Michigan
Institute for Plasma Science & Engr.
t = 0.1 – 0.12 s
Achieved tmax
Crystallizing
Animation
tmax increases by 30% from cw to 0.5 DC pulsed (0.035 to 0.045 s).
Shorter DC extends crystallization limit.
tmax for DC of 0.3, 0.5, and 0.7 are 54, 45 and 43 ms.
For shorter DC, stronger NP heating during power-on outweighs the lowered heating during power-off.
Notes: 19

## Slide 20
CONCLUDING REMARKS
University of Michigan
Institute for Plasma Science & Engr.
  Compared to CCPs, ICPs can crystallize larger NPs but tmax is short due to the higher growth rate.
  Pulsed ICP extends the crystallization size limit, resulting in more efficient NC production.
  Lower DC for pulsed ICP improves NC production.
  Optimization of plasma reactors for NC production requires consideration of not only plasma density, but other factors such as NP growth rate, charge and trapping locations as well.
  Mixing operating conditions (cw + pulsed) may be beneficial to NC synthesis.
Notes: 20