## Slide 1
Multiscale Modeling of Radical and Vibrational Pathways in Plasma-Assisted Ammonia Synthesis on Fe(110) and Ni(111)
Oluwatosin A. Ohiro*, Samuel A. Ogunwale, Bryan R. Goldsmith
Department of Chemical Engineering, University of Michigan, Ann Arbor, MI, 48104, USA
Background and Motivation
Modeling Methodology
The Haber–Bosch process for ammonia (NH3(g)) synthesis is responsible for 1–2% of global energy consumption[1]
New catalytic technology is needed for sustainable ammonia synthesis
Low temperature plasma (LTP) assisted catalysis is a potential complement to traditional thermocatalytic chemical conversion processes, such as NH3(g) synthesis.[2]
Activate difficult molecules (e.g., N2) and enhance reactivity at low temperature
Z*
X*
X*
Active Site/Vacancies
Eley–Rideal reaction
Langmuir–Hinshelwood
reaction
Micro-discharge
Electric Field
Enhancements
Plasma–catalyst Interactions
Gas phase reactions
X*
X
Y*
X*
Y*
Z
ions
vibrationally excited
species X(𝑣)
molecule
radicals
electron
Complex interactions affect elucidation of the mechanism for LTP-assisted NH3(g) synthesis[1]
Understanding interactions in LTP system allows for optimization of reaction conditions, catalyst type, and energy/environmental considerations
We study plasma species generated in RF reactor interactions in a packed bed reactor (PBR)
We compare 5 microkinetic models increasing complexity to elucidate how different species affect the rate of NH3 formation and examine which model rationalizes our experiments on Fe and Ni catalysts
Model parameters are computed via density functional theory (DFT) and mean-field microkinetic models are constructed to compare to experiments results.
Reactions
Transient flow behavior in a PBR
Electronic energy
Free Energy
Many-body
problem
Experiment
Reaction
Conditions
(T,P)
Microkinetic modelling
Model Comparison with Experiment
DFT
Goal: Elucidate how various LTP-generated species yield
similar NH3 rates across different metal catalyst
Figure 5. Reaction rate kinetics involving LTP generated species interaction with surface metal catalyst on Fe (110) at 517 K and 1 bar. Blue bars represents the forward rate constants, while the gray bars represents the reverse reaction rates.
Reaction Mechanism Elucidation Results
Figure 6. NH3(g) densities at the outlet of the PBR reactor on Fe(110) and Ni (111) metal surface. Operating conditions: 1 atm, 517 K, 1 SLM total flow rate. Feed gas composition: 0.5% N2(g), 2.5% H2(g), 97 % Ar(g). LTP species are generated in the upstream RF plasma reactor before entering the PBR. N• densities = 11014 cm−3, H• densities = 11016 cm−3.
Initial computational results show orders of magnitude differences in NH3(g) production when only N2(g), are consider only. High vibrational levels with lower dissociation barriers lead to higher reaction rate for NH3(g)
The identity of most active metal for NH3(g) synthesis changes from prior computational analysis
Experimental results show similar orders of magnitude of NH3(g) production across metals
Rate constant analysis reveals that highly vibrationally excited N2(g), may not be active during the reaction due to surface quenching reactions
Figure 2. Comparison of distribution-weighted (plasma-on) and thermal (plasma-off) NH3(g).[3]
From thermodynamics
Forward rate constants
Backward rate constants
… for N2(g), dissociation
Langmuir Hinshelwood reactions
Eley-Rideal Reactions
Equilibrium rate constant are obtained from each chemical reaction
Reaction Rate
1
2
3
4
5
6
(a) Thermal
(b) N2(g),
(c) N2(g),+ N•
(d) H2(g)+ H•
(e) N2(g),+H2(g)+ N• + H•
N2(g)
H2(g)
Ar(g)
Catalyst
MBMS
10 mm
Catalyst
MBMS
N2(g)
Ar(g)
N2(g),
H2(g)
Catalyst
MBMS
N2(g)
Ar(g)
H2(g)
N2(g),
N(g)
N(g)
Catalyst
MBMS
H2(g)
Ar(g)
N2(g)
H2(g)
H(g)
N2(g)
H2(g)
Ar(g)
Catalyst
MBMS
H(g)
N2(g),
N(g)
H2(g)
Figure 8. (a, b) Gas densities along the length of the PBR on (a) Fe and (b) Ni catalyst. Vibrationally excited N2(g), are shown in grayscale, only the first six vibrational levels are shown for visual clarity. (c, d) Elementary reaction rates along the reactor. Langmuir Hensel wood reactions are in grey, E-R reations are in blue on (c) Fe and (d) Ni. Operating conditions: 1 atm, 517 K, 1 SLM total flow rate. Feed gas composition: 0.5% N2(g), 2.5% H2(g), 97 % Ar(g). LTP species are generated in the upstream RF plasma reactor before entering the catalytic bed. N• densities = 11014 cm−3, H• densities = 11016 cm−3.
(b)
(a)
(d)
(c)
Fe shows better performance compared to Ni as expected under pure thermal catalysis
Ni performance improves due to easier nitrogen fixation on the catalyst surface from N2(g),
Fe turnover rate is improved in the presence of H radicals, indicating that thermal NH3(g) production is limited due to the absence of H radicals.
We achieve parity in metal performance when all limiting reactants are indued in the model
A synergistic effect is seen in overall NH3(g) density when all LTP-generated species are included in the model (i.e. N2(g),+H2(g)+ N• + H•)
Faster Eley–Rideal kinetics dominate reaction pathway for NH3(g) production
H• are consumed at a much faster rate than N• densities. When present, H• become the dominant source of hydrogenation.
Increase in N2(g),=0 at reactor outlet is due to quenching reaction of higher excited states and recombination of N•
[1] Sun, J.; Alam, D.; Daiyan, R.; Masood, H.; Zhang, T.; Zhou, R.; J. Cullen, P.; C. Lovell, E.; Ali Jalili; Amal, R. Energy Environ. Sci. 2021
[2] Bogaerts, A.; Tu, X.; Whitehead, J. C.; Centi, G.; Lefferts, L.; Guaitella, O.; Azzolina-Jury, F.; Kim, H.-H.; Murphy, A. B.; Schneider, W. F.; Nozaki, T.; Hicks, J. C.; Rousseau, A.; Thevenet, F.; Khacef, A.; Carreon, M. J. Phys. Appl. Phys. 2020.
[3] Mehta, P.; Barboun, P. M.; Engelmann, Y.; Go, D. B.; Bogaerts, A.; Schneider, W. F.; Hicks, J. C. ACS Catal. 2020
[4] Bayer, B. N.; Raskar, S.; Adamovich, I. V.; Bruggeman, P. J.; Bhan, A. Plasma Sources Sci. Technol. 2023
Figure 7. NH3(g) densities at the outlet of the PBR reactor on Fe(110) and Ni (111) metal surface at various LTP RF power for Model N2(g),+ N• and Model H2(g)+ H•. Operating conditions: 1 atm, 517 K, 1 SLM total flow rate. Feed gas composition: 0.5% N2(g), 2.5% H2(g), 97 % Ar(g).
References
Uncertainty in Species Activity for NH3(g) Synthesis
Figure 3. Measured NH3(g) STYs in the DBD reactor on metal/Al2O3 catalysts as a function of the DFT-calculated nitrogen adsorption energy. T = 438 K.[3]
Figure 4. Upper bounds on the ratio of rates of dissociative adsorption to the rates of N2() over Fe, Ni, and Ag metal wool catalysts as a function of vibrational level at the experimental surface temperature
Increasing model complexity to include Eley-Rideal reactions reconciles the discrepancy between experimental and computational results for Fe and Ni catalysts.
Similar analyses should be conducted across other transition metals to determine whether these trends persist more generally.
Conclusions
Eley–Rideal Reactions
Langmuir–Hinshelwood Reactions
Notes: Fe and Ni catalyst are sensitive to the nature of the LTP species.
Fe turnover rate is improved in the presence of H radicals Figure X. indicating that thermal NH3 production on it is limited due to the abbsece of H radicals.
Ni improves die to easier nitrogen fixation on the catalyst surface
We achieve parairty in metal perfomacne when all LTP generated species are included in the model (i.e. N2(g),+H2(g)+ N• + H•)
Synegistic effect is seen in overall NH3 density in the when both radical species are present
Fe and Ni catalyst are sensitive to the nature of the LTP species.
Fe turnover rate is improved in the presence of H radicals Figure X. indicating that thermal NH3 production on it is limited due to the abbsece of H radicals.
Ni improves die to easier nitrogen fixation on the catalyst surface
We achieve parairty in metal perfomacne when all LTP generated species are included in the model (i.e. N2(g),𝜈+H2(g) + N• + H•)
Synegistic effect is seen in overall NH3 density in the when both radical species are present