## Slide 1
Javad Mostaghimi
Centre for Advanced Coating Technologies
University of Toronto
Toronto, Ontario, CANADA
Dynamics of Droplet Impact &
Solidification in Plasma Spray Process
Michigan Institute for Plasma Science & Engineering
April 6, 2011

## Slide 2: Thermal Spray Processing
Thermal spray coatings protect surfaces against corrosion, wear, high temperature
Coating materials: metals, ceramics, cermets, polymers

## Slide 3: Coating Microstructure
VOID
OXIDE
INCLUSION
UNMELTED
PARTICLE
SUBSTRATE
After Sulzer-Metco

## Slide 4: Coating Formation
Diameter D0
Impact Speed V0
Density r
Viscosity m
Surface Tension Coeff. s
Specific Heat C
Heat of Fusion Hf
Substrate Temperature Ts
Melting Point Temperature Tm
Needed Information:
Particle size distribution
Particle impact velocity distribution
Particle temperature distribution
Torch trajectory

## Slide 5: Dimensionless Parameters
Fluid Mechanics
Reynolds Number Re = rVoDo/m (viscosity)
Weber Number We = rVo2 Do/s (surface tension)
Heat Transfer
Stefan Number Ste = C (Tm-Ts)/Hf (solidification)
Prandtl Number Pr = n/a (material property)

## Slide 6: Capillary Effects
Maximum Spread factor is shown to follow the following relationship (Pasandideh et al, Phys. Fluids, 1996)
where:
For:
the values of contact angle are not necessary. When
= 0.5

## Slide 7: Formation of Pores
The sources of porosity formation:
  Curl up
  Un-melted particles
  Incomplete filling of interstices
86 µm

## Slide 8: Example of Coating Deposition
Process parameters | Mean Value | Standard deviation
Velocity V [m/s] | 60 | 5.7
Diameter D [ ] | 58 | 18
Temperature T [K] | 1882 | 219
Dispersion Angle [degrees] | 0 | 0.5
Azimuthal angle [degrees] | 0 | Uniform distribution from
Edge curl-up angle [radians] | 5h/(4d) | 5h/(24d)
Input parameters to the model
Powder mass flow rate: 1 lb/hr;
Gun speed along the x direction: 0.5m/s
Gun passages: 14.

## Slide 9: Sample Results
The 3-D microstructure result of one simulation with stand off distance of 150mm
Porosity=14%
x=1 mm cross section.
Average thickness=154 mm
Average roughness=11 mm

## Slide 10: Nickel on Stainless Steel

## Slide 11
Coating cross-section of three cases from NRC-IMI: (a) experiment
(b) Stochastic model

## Slide 12: Thermal Spray Sources
DC plasma
RF Inductively Coupled Plasmas
High Velocity Oxy-Fuel (HVOF)
Flame spray
Wire-arc spray

## Slide 13: Spray Sources
RF-ICP
DC
Wire-Arc
HVOF

## Slide 14: Splats
500 mm Wire arc
Plasma
To increase adhesion, prior to spraying, the component is grit blasted resulting in roughness of about 3 microns.

## Slide 15: Microstructure
Coatings are an accumulation of many lamellae or “splats”.
Micrographs of (a) an individual splat on a substrate, (b) coating cross-section, (c) lamellae close up.
4 mm
(c)
60 mm
(b)
(a)
80 mm

## Slide 16: Motivation
Coating properties, e.g., porosity and adhesion strength, and its microstructure depend on:
    Particle impact conditions (velocity, temperature, impact angle)
    Substrate temperature
    Roughness
    Materials properties of powder and substrate
Fundamental understanding of fluid flow and heat transfer during the impact is crucial in improving the processes

## Slide 17: Impact Conditions
Microstructure of coatings strongly depends on:
  Particle impact conditions
  Substrate conditions
25°C
300°C

## Slide 18: Ni on Stainless Steel
290 oC
340 oC

## Slide 19: Splat Shapes
Splat shapes depend on many parameters, including:
  Impact conditions, i.e., speed, size, impact angle
  Particle properties which depend on the type of material and its temperature
  Substrate conditions, which depends on the substrate material, roughness, and substrate temperature

## Slide 20: Droplet Impact and Solidification

## Slide 21: Mathematical Modelling
Basic Assumptions
  laminar and incompressible fluid flow
  solidification at the equilibrium temperature (Tm)
Governing Equations
  Flow: - continuity and momentum equations
  Energy: - enthalpy method for fluid region - heat conduction within substrate
  Surface tracking methods (VOF, LS, CLSVOF, advecting normals)
Thermal contact resistance is considered

## Slide 22: Governing Equations Conservation of Mass and Momentum

## Slide 23: Energy Equation Enthalpy Method
with the following conditions at the solidification front:
substrate
liquid
    solid

## Slide 24: Pressure Jump at the Interface
At the Free Surface
where…
Plasma
Liquid
Q
For a spherical drop
k = 2/R

## Slide 25: Tracking the Interface: Volume-of-Fluid Method
Define VOF function:
Governing equation:

## Slide 26: Comparison with Experiment
0.0 ms
0.4 ms
1.2 ms
1.6 ms
2.4 ms
3.2 ms
4.0 ms
3 mm offset

## Slide 27: Droplet Impact

## Slide 28: Nickel Splat Shapes
  Droplet : 60 µm, 73 m/s, 1600 oC
  Substrate: 290 oC

## Slide 29: Nickel Splat Shapes
  Droplet : 60 µm, 73 m/s, 1600 oC
  Substrate: 400 oC
Rc=10-6 m2K/W

## Slide 30: Two-droplet splats
  Nickel particle : 60 µm, 48 m/s, 2050 oC
Rc=5x10-7 m2K/W

## Slide 31: Multiple Impacts

## Slide 32: Findings
The model demonstrates the important effects of droplet impact conditions, its properties and the substrate conditions in determining the final shape of a splat
It is clear that superheating of a droplet, which results in lowering viscosity, is beneficial
Plasma sources that can heat and melt the powders more effectively should therefore produce better coatings

## Slide 33: A New DC Plasma Torch
An ideal plasma torch will have: high thermal efficiency, high thermal conductivity, and high enthalpy
One way to achieve this would be to use CO2/CH4 gas mixture
Two issues:
  Because of the presence of oxygen we cannot use W cathodes,
  There will be deposition of carbon ions on the cathodes
  This suggests that we may use graphite cathodes

## Slide 34: CO2/CH4 vs. Argon Properties
Composition
Enthalpy
Thermal
conductivity
Employing CO2/CH4 as plasma gas should result on the deposition of C+ on the cathode.

## Slide 35: DC Plasma

## Slide 36: Graphite cathode
Spectroscopic measurements show that plasma temperature near graphite cathode surface is about 12,000K.
At this position carbon is ionized to about 30%.
The cathode surface is at ~4,000 K.
For graphite cathodes operating in Ar, measured erosion rate was from 3.5 to 10 mg/C (J. Haidar , Plasma Sources Sci. Technol. 5 ,1996)
Graphite cathode

## Slide 37: Cathode Formation
Excessive carbon deposit in Ar+CH4 gas mixture destabilizes the arc
Deposit diameter ~6 mm
Cathode surface formed by ion current

## Slide 38: Cathode formation
Cathode after several hours in
service (power 30-45 kW)
For CO2 + CH4 gas mixture,
due to the presence of CO2, excessive carbon is oxidized and the deposit has stable and confined disc-like shape
diameter ~3mm

## Slide 39: Cathode Formation
Cathode surface structure
SEM micrographs

## Slide 40: CACT Torch – Low Power
Cathode: Graphite, W, Hf
Anode: Copper
Gases: CO2 based mixtures, Ar, Air
Power range ~ 30-70 kW
Arc Current ≤ 400A
Arc voltage 130-220V
Thermal efficiency 60-85%.

## Slide 41: CACT Torch - High Power
Magnetically rotating anode root
The coil was excited in series with the anode
Benefits:
Anode heat load is distributed over large area and this way reduces anode erosion
Arc rotation provides more uniform heating large gas volumes
Arc voltage is higher so that more power can be introduced to the gas at a given current
Notes: Magnetic field at the cathode region (Linde 1930-es)
Cathode and anode spot rotation by Westinghaus for NASA heaters

## Slide 42: High power torch
For materials processing and waste treatment, or large powder feed rate (~ 30 kg/hour) higher power torch with larger plasma volumes is needed.
Power up to 200 kW
thermal efficiency 60-80%
gas flow up to 200 lpm
Visible plume length 50 cm

## Slide 43: Voltage Fluctuations
Chart: I-V characteristics
| 400 | 350 | 300 | 300 | 250 | 220 | 200
High power torch | 246 | 260 | 262 | 253 | 269 | 286 | 297
Low power torch | 154.4 | 154 | 148.7 | 142.2
Vavrg 167.5
STDV 5.12
I=300A
Vavrg 153.2
STDV 23.3

## Slide 44: Y2O3 Coatings (Low Power Torch)
Torch | Gas flow, lpm | Current A | Voltage V | Power kW | Thermal efficiency %
SG-100 | 40 (Ar) 8 (He) | 750 | 45 | 33.8 | 35.2
CACT | 35 (CO2) 14 (CH4) | 300 | 120 | 36 | 56
For SG-100 torch spray parameters and distance of 120 mm were adopted from work by J.Kitamura et.al [1]
The CACT torch parameters were adjusted for comparable input power and gas flow rate
Powder:
Y2O3 9271 (Saint-Gobain),
particle size +10-63 μm
Feed rate 5 g/min
S3091 (Inframat)
9271 (St-Gobain)
Fujimi [1]
1 Kitamura, H. Hiroyki, F. Yuasa, H. Mizuno JTST 17, 2008. pp. 878-886.

## Slide 45: Yttria Splats
CACT torch
Particle: T= 2697 oC, V= 112 m/s
SG-100
Particles: T= 2573 oC, V=102 m/s.
Splats were collected on polished stainless steel substrate

## Slide 46: Particle conditions
Y2O3 Tm = 2440 °C
particle conditions along the torch centerline
(DPV 2000)
Distance | Particle parameter | SG-100 | CACT
100 | T, °C | 2535 | 2744
 | V, m/s | 92 | 120
120 | T, °C | 2573 | 2697
 | V, m/s | 102 | 114

## Slide 47: Yttria Coatings
Total 24 passes | Coating thickness μm | Deposited mass kg/m2 | Porosity % | 
SG100 | 80 | 0.37 | top layer 4.3 | 
CACT | 430 | 1.87 | 8.6 | 
SG100
CACT

## Slide 48: Conclusions
The new plasma torch heats the powders to higher temperatures than Ar/He or Ar/H2 torches
The result is a higher degree of superheat, round splats, and importantly, much higher deposition efficiency
Thermal efficiency of this torch is between 60% to 80%

## Slide 49: Thank You!