## Slide 1
Electron-beam generated plasmas and their applications: from materials processing to space propulsion
Yevgeny Raitses
Princeton Plasma Physics Laboratory
MIPSE, Ann Arbor, MI
February 7, 2024

## Slide 2
Alex Likhanskii, Leonid Dorf, and Andrei Khomenko
Nirbhav Chopra, Ivan Romadanov, Eduardo Rodrigues, Jacob Simmonds, Shurik Yatom, Igor Kaganovich, Santosh Kondeti, Sophia Gershman
Fang Zhao and Chris Tully (Phys.), Arthur Dogariu and Mikhail Shneider (MAE)
Scott Walton, Lina Petrova, and David Boris
Kai-Mei Fu and Christian Pederson
Andrei Smolyakov
Junhwi Bak and Gerardo Urdaneta Rincon

## Slide 3
Synopsis
Electron beam generated plasma, intro
  Focus on sub-10 keV, low power (< 1 kW), low current density < 1 A/cm2
  Main applications: materials processing (e.g. ALE, ALD, polymer processing, )
Electron beams in our research
    Princeton Collaborative Research Facility (PCRF)
    Microelectronics and Quantum Information Systems (QIS)
    Plasma propulsion
Takeaway notes
3
Notes: 3

## Slide 4
E-beam generated low temperature plasma
cathode
beam dump
(electron collector) or repeller)
E
ions
e-beam
plasma
Energy relaxation length in inelastic range
For 2 keV in 50 mtorr N2 with neutral density N (m-3)
Energy loss function
e-Beam required to generate the plasma
Wall losses
Ionization by e-beam
e-Beam plasma without magnetic field
Beam electrons scattered on collisions with neutrals causing the beam expansion
R. F. Fernsler, W. M. Manheimer, R. A. Meger, et al., Phys. Plasmas 9 (1998)
Substrate for plasma treatment
S. Macheret, M. Shneider, R. Miles, Phys. Plasmas 13 (2006)
ions
electrons
Notes: 4

## Slide 5
Examples of e-beam plasma systems without B-field
K. D. Schatz and D. N. Ruzic Plasma Sources Sci. Technol. 2 (1993)
M. J. Kushner, W. Z. Collison, and D. N. Ruzic, J. Vac. Sci. Technol. A 14 (1996)
J. Jung et al., Phys. Plasmas 30 (2023)
A S Klimov et al., Phys. Plasmas 25 (2018)
70 cm, 10 keV, 0.3 torr He
C. Lee et al., J. Vac. Sci. Technol. A 38 (2020)
100 eV
2-100 mtorr
Ar, O2/CF4
1.5-2 keV
30 mA
50 mtorr
Ar, O2
< 30 eV
3 mtorr
Ar, O2
Notes: 5

## Slide 6
e-Beam plasma systems with B-field
thermionic
Applied B-field reduces the spread of beam electrons by collisions with neutral atoms:
W. M. Manheimer et al., Plasma Sources Sci. Technol. 9 (2000)
S. Walton et al., Surf. Coat. Technol 186 (2004)
0.1-10 mtorr
Ar, Xe, Kr
< 60 eV
10-1000 Gauss
~ 1-3 A
E. Rodriquez et al., Phys. Plasmas 26 (2019)
1-10’s mtorr
Ar, N2 O2
2-4 keV
100 Gauss
~ 1-20 mA
Y. Sakawa et al., Phys. Fluids B 5 (1993)
Notes: 6

## Slide 7
Different regimes with different sources of e-beam
Ion-Induced Secondary Electron Emission Cathode, (NRL, UIUC, Tomsk)
Thermionic Cathode (e.g. hot filament or disk), (UCLA, PPPL etc)
DC-RF (ICP) Plasma Cathode (PPPL)
Cathode type | Energy, keV | Current density, mA/cm2 | Pressure, torr
iSEE | 1-10 | 1-10 | 10-3-10-1
DC-RF | <0.1 | 103 | 10-4-10-2
Thermionic |  0.1 | 10-3-104 | 10-8 -10-2
Also, plasma hollow cathodes….(e.g. NRL, Oks’s group)
Notes: 7

## Slide 8
Different electron sources=> Different dominant reactions
* Adapted from S. Walton et al., Surf. Coat. Technol 186 (2004)
iSEE
Thermionic
DC-RF
From Ref. *, Electron impact excitation, dissociation, and ionization cross sections for N2
Cold cathode, (iSEE)
Hot cathode
(thermionic)
DC-RF cathode
Notes: 8

## Slide 9
Beam-plasma instabilities
The (two-steam) stability criterion
R. F. Fernsler, et al., Phys. Plasmas 9 (1998)
More detail studies including PIC simulations
H. Son et al., Phys. Rev. E 106 (2022)
Jb ~ 70 mA/cm2, 4 keV, and 50 mtorr
Q. Cao, J. Chen, Phys. Plasmas 30 (2023)
N. Chopra et al., in preparation
To mitigate beam-plasma instabilities, increase velocity spread of beam electrons,
R. J. Briggs, Adv. Plasma Phys. 4 (1971)
Notes: 9

## Slide 10
Princeton Collaborative Research Facility (PCRF)
Experts in plasma theory, computational, experiments and diagnostics
Advanced diagnostics of plasma, gas flow, nanoparticles, plasma-surface interactions
Wide range of plasma sources for basic and applied research
Mist-plasma jets
Low pressure ExB plasma
Arc discharges
e-beam generated LTPs: low to moderate (~ torr) pressures
Facilities at PPPL and Princeton > 5000 sq.ft and more coming
3-D PIC: ExB plasma structures
Basic LTP science
Plasma-surface interactions relevant to advanced processing
Plasma-liquid interactions
Nanosynthesis and dusty plasmas
Advanced computational resources: 2D, 3D codes, HPC: CPU-GPU hybrid architecture with open-source codes
http/pcrf.pppl.gov
Since 2019, 88 user projects
Notes: 10

## Slide 11
PCRF user and host projects on e-beam generated plasmas
Probing metastable species in e-beam generated plasmas User PI: Scott Walton, NRL and Host projects: S. Kondeti, S. Yatom
Electrostatic wave-wave interactions in e-beam plasma, Host project: I. Kaganovich
LIF results
PIC simulations of e-beam plasmas
Host projects: I. Kaganovich, W. Villafana, in collaboration with Shahid Rauf, AMAT
Control of EEDF in e-beam plasmas
Host project: Y. Raitses and N. Chopra
Cold Hydrogen Plasma Passivation for Quantum Defect Charge State Control, User PI: Kai-Mei Fu, Univ. of Washington
Plasma based hydrogen doping of semiconductors for color center qubit optimization, User PI: T. Schenkel, LBNL

## Slide 12: Microelectronics and QIS research at PPPL
PPPL is expanding into research on understanding plasma processes required for creating the next generation of semiconductors and QIS materials, advancing the nation’s push to shape the future of computing.
One of thrusts: noninvasive diagnostics of processing plasmas and plasma-surface interactions in state-of-the-art industrial reactors
Focus:
Plasma stoichiometry: spatially (~ 102m) and temporarily (~ s) resolved diagnostics
Kinetic properties of the plasma: velocity distribution functions of electrons, ions, atoms
1-D and 2-D structured light diagnostics with minimum access requirements (e.g. confocal)
In situ surface properties (e.g. charging, chemistry)

## Slide 13: PPPL –Applied Materials Inc. collaboration
Pulsed Argon plasma source at 10’s mtorr
LIF excitation: 696.5 nm, 8 J/pulse, ~10 ns,100 Hz, laser linewidth < 50 pm
LIF Fluorescence: 727.5 nm
Santosh Kondeti
PPPL researcher
at AMAT, CA
PPPL advanced optical diagnostics installed and applied for plasma etch research at AMAT, Santa Clara, CA
Kondeti et al., in preparation

## Slide 14: Advanced laser diagnostics for industrial plasma reactors
A strong need in spatially and temporally resolved plasma diagnostics suitable for real industrial processing reactors
Limited diagnostic access on industrial reactors due to complex geometry, uniformity perturbation, and harsh environments
Conventional Laser-Induced Fluorescence (LIF) configuration
Not applicable
For best spatial resolution, need two optical view ports at 90 deg!

## Slide 15: Confocal laser diagnostics for industrial plasma reactors
I. Romadanov and Y. Raitses, Rev. Sci. Instrum. 97, 073002 (2023)
Good agreement between IVDFs measured with confocal and conventional LIF configurations
Plasma volume
collection optics
Detector
axicon 1
axicon 2
Collected light
Tunable Diode Laser
&
Beam conditioning
Electronics
Dichroic mirror
lens
Optical access port
laser beam profile
Ion Velocity Distribution Function (IVDF)
confocal vs conventional
Confocal LIF – need only 1 viewport!

## Slide 16
Insights of ion transport in e-beam plasma using probes & LIF
Property | Value
Ar gas pressure | 0.1 mTorr
-field | G
Beam energy | ~ 50 eV
Beam current | ~ 100 mA
Property | Value
Ar gas pressure | 0.1 mTorr
Beam energy | ~ 50 eV
Beam current | ~ 100 mA
Plasma diagnostics:
  Langmuir probe EEDF ->
  Emissive probe plasma potential
  LIF and VDFs
Chopra, Romadanov, Raitses, Appl. Phys. Lett. 124 (2024)
Notes: 16

## Slide 17
Probe results: Ion trapping in e-beam plasma region
Consistent with Sakawa, Chen et al., Phys. Fluids B: Plasma Phys. 5, (1993)
Plasma density, electron temperature, plasma potential, and ionization rate
Electric field direct ions towards the source axis, away from the chamber wall
Notes: 17

## Slide 18
LIF results: Ion heating in e-beam plasma region
Ions are born at different places of the potential well causing the ion energy spread - effective ion heating?
Chopra, Romadanov, Raitses, Appl. Phys. Lett. 124 (2024)
Warm ions can diffuse against E-field, towards the chamber walls (anode), forming ion backflux.
Notes: 18

## Slide 19
Other possible mechanisms of ion heating
Heating from collective effects, plasma instabilities:
  Counter-streaming unmagnetized ion populations generated in the radial potential well with magnetized electrons → Lower hybrid instability
e-Beam-plasma instabilities
Mikellides et al., J. Appl. Phys. 129 (2021)
Sun, Chen, Kaganovich et al, Phys. Rev. Lett. 129 (2022)
Phys. Rev. E 106 (2022)
Ion heating in 2D PIC simulations of e-beam ExB plasma (Penning)
Tyushev et al., Phys. Plasmas 30 (2023)
Work in progress: experimentally characterizing instabilities in e-beam ExB plasma
Notes: 19

## Slide 20
“Gentle” processing/doping of 2D with e-Beam ExB Plasma
e-beam ExB plasma, graphene hydrogenation
Demonstrated the highest H coverage (~38%) of graphene by plasma and no damage to graphene!
Zhao, Raitses et al., Carbon, 177 244 (2021)
B-field effects:
Backflux of warm ions (and partially by cold ions from CEX) and neutrals (CEX) contributes to processing by all e-beam plasma systems.
H-coverage of graphene from ex-situ Raman
H-density in plasma by fs-TALIF
Notes: 20

## Slide 21
N. De Leon
Qubit performance 🡨🡪 Materials properties 🡨🡪 Plasma-surface interactions 🡨🡪 RF/Plasma-chemistry
(dopants)
Ashfold et al., 2020
Oberg, Stacey, et al, 2021
Plasma diagnostics
Plasma modeling
Plasma/surface modeling
Synthesis experiments
Material/device delivery
Quantum & Microelectronics Diamond
PPPL/Princeton University co-PIs: Alastair Stacey, Nathalie de Leon, David Graves, Igor Kaganovich, Yevgeny Raitses

## Slide 22
Hydrogen passivation of diamond with e-beam ExB plasma
The same e-beam ExB plasma for QIS materials: diamond, silicon
Ex-situ evaluation of H passivation of diamond surface and color centers
Prof. Kai-Mei Fu’s group at UW
Christian Pederson et al., submitted (2023)
No irreversible damage to diamond surface
Notes: 22
a) Measurement of the wetting angle indicating a shift from hydrophilic to hydrophobic surface upon exposure to hydrogen
plasma, confirming hydrogen surface termination after plasma treatment. b) Atomic force microscopy (AFM) images showing negligible
change in the diamond surface roughness due to plasma exposure. c) Confocal microscopy images obtained with 532 nm laser excitation,
600-900 nm collection, showing PL from implanted NV and SiV defect centers. Post plasma exposure, shallow defects (15 nm from
surface) are not detected and deeper defects (60 nm from surface) exhibit reduced PL intensity, indicating a shift to an undetected charge
state. d) Comparison of PL spectra from the deeper defects confirms a change in the NV defect charge state after plasma exposure.

## Slide 23
1999
2022
2nd International Congress on Aeronautics, London, UK, 1952
http://htx.pppl.gov
Plasma propulsion research at PPPL
Hall Thruster Experiment (HTX) in 1998 by N.J. Fisch and Y. Raitses and graduate students L. Dorf, A. Smirnov, A. Litvak and D. Staack
Focus: Understanding of fundamental limitations of ExB plasma thrusters
23

## Slide 24
A need exists for a spacecraft to occupy a very low orbit at altitudes of 100 - 200 km: Earth observation, telecommunication, science
The challenge is to overcome air drag as the air densities are not insignificant.
ESA air scoop –air Hall thruster for operation in 200 km orbit. http://www.esa.int/spaceinimages/Images/2018/03/Air-breathing_ion_thruster
Airbreathing plasma propulsion
For this spacecraft to be parked in this orbit indefinitely, the propellant need to be harvested from the surrounding atmosphere.
24

## Slide 25
Drag power,
vs
Interested in low altitudes of 90-200 km
Extreme power requires for < 130 -150 km
Compression, , increases power requirements.
Challenge # 1: Power requirement
25

## Slide 26
At 100-200 km, N2 and atomic O key components
More energy needed on electron impact ionization of N2 and O than on traditional EP propellants (Xe, Kr)
Negative ions of oxygen can make it harder to initiate and maintain plasma
Chemical erosion of thruster by atomic and ionic oxygen and nitrogen species
Harder to generate the thrust with lighter N and O than with Xe and Kr
Challenge # 2: Ambient air propellant
1 mtorr
26

## Slide 27
The minimum energy cost: 66 eV – close to the Paschen minimum
The lowest energy cost is for electron beam, 34 eV (model and experiments)1,2
For non-beam EEDF or e-beam > 34 eV, energy cost is higher due to energy losses on excitation etc.
DC glow, RF- plasmas are fundamentally inefficient for ionization of air.
Solution: ionization by electron beams
Ionization cost for air,
1 Bychkov, Vasilev, Zuev, High Temperature 32 (1994)
2 Macheret, Shneider, Miles, Phys. Plasmas 13 (2006)
E-beam plasma as a solution to challenges # 1 and 2
27
Notes: 27

## Slide 28
From rate balance equation for e-beam ionization source,*
Plasma wall losses
-Wall flux:
-Flux of accelerated ions:
E-beam power, W
e-Beam requirements for thrust = drag compensation
Plasma accelerated out
Beam power needed to generated the required plasma density (to generate the thrust):
*W. M. Manheimer, R. F. Fernsler, M. Lampe and R. A. Meger, PSST 9 (2000)
28
Notes: 28

## Slide 29
Ionization of incoming air by magnetically confined e-beams and ion acceleration like in cylindrical Hall thruster (in diverging B-field)
Airbreathing e-Beam plasma thruster concept
Raitses, Simmonds, Chopra, IEPC-2022- 443
Raitses and Fisch, Phys. Plasmas 8 (2001)
Kornfeld et al., IEPC (2003)
29
Notes: 29

## Slide 30
FFI
EB rotating plasma structures
Probes
5 kHz
Almost 100% of the electron current across the magnetic field through the spoke
Skoutnev et al., Rev. Sci. Instrum. 89 (2018)
Powis et al., Phys. Plasmas 25 (2018)
Rodriguez et al., Phys. Plasmas 26, (2019)
Experiment, Xenon, 0.1 mtorr
PIC simulations (no ionization)
30

## Slide 31
Gradient drift instability: collisionless Simon-Hoh instability
Equilibrium
Density perturbation
Perturbation
A. Smolyakov et al., Phys. Plasmas 20 (2013)
Instability growth rate
Heating of electrons in the spoke may enhance ionization
  Conditions: neo  0 and neo  Er0 > 0
Wci << w << Wce
31
Notes: 31

## Slide 32: Short-circuit effect of the boundaries
Measured time-averaged plasma properties
With conductive boundaries the electric field is greatly reduced.
Rodriguez et al., Phys. Plasmas 26 (2019)
Conductive wall
Insulating side walls
Instability growth rate
32

## Slide 33: Suppression of oscillations
Oscillations of the plasma density
Rodriguez et al., Phys. Plasmas 26 (2019)
33

## Slide 34
A 70 cm long e-beam with a thermionic cathode operating in N2 atmosphere, 0.1 microtorr
Initial experiments with e-beams in Nitrogen and Air
Normalized electron energy distribution function (EEDF) at the beam injection and collection
heating of plasma electrons?
Torr
mA
60V
.
Mostly molecular N2 ions
34
Notes: 34

## Slide 35
Take away messages about e-beam plasmas
Sub keV e-beams for controllable production of ions & radicals for semiconductor and QIS materials processing (e.g. ALE, 2D materials, diamond)
  High current density DC-RF cathodes as the source of non-thermal electrons
New physics insights with advanced diagnostics and modern computational tools:
  Ion heating in the potential wall and the back ion flux to the substrate
  Suppression of gradient drift instability in ExB fields by short circuit on boundaries
  New regimes predicted for beam-plasma instabilities
Potential application for plasma propulsion with molecular propellants (e.g. airbreathing)
35
Notes: 35

## Slide 36
Acknowledgement
The work supported by the US DOE under Contract No. DEAC02-09CH11466 and by the Air Force Office of Scientific Research
36
Notes: 36

## Slide 37
Alex Likhanskii, Leonid Dorf, and Andrei Khomenko
Nirbhav Chopra, Ivan Romadanov, Eduardo Rodrigues, Jacob Simmonds, Shurik Yatom, Igor Kaganovich, Santosh Kondeti, Sophia Gershman
Fang Zhao & Chris Tully (Phys.), Arthur Dogariu and Mikhail Shneider (MAE)
Scott Walton, Lina Petrova, and David Boris
Kai-Mei Fu and Christian Pederson
Andrei Smolyakov
Junhwi Bak and Gerardo Urdaneta Rincon
37

## Slide 38
Backup slides
38

## Slide 39
Argon Metastable LIF: Setup and Transition Scheme
Transition scheme
Experimental setup
LIF Signal
S. Kondeti, S. Yatom, N. Chopra, Y. Raitses
(11.55 eV)
Notes: Population dynamics is driven by laser-induced excitation from level 1 to level 2, laser-induced de-excitation from level 2 to level 1, spontaneous photo-relaxation from level 2 to levels 1,3,4 and 5 and radiation-less relaxation from level 2.
The quantification of the Ar metastable density at level 1s5 from the measured LIF signal requires instrumental values, specific to the given optical setup and sensor as well as modeling the population dynamics of excited levels following the laser excitation of the 1s5 .

## Slide 40: Changing Ar* Metastable Density with Addition of N2
Averaged density in the center
P=60 mTorr , B=100 G
N2 (%) | I(mA) | P_Ar (mTorr) | P_N2 (mTorr)
0 | 3.6 | 60 | 0
1.8 | 3.8 | 59.14 | 1.08
2.82 | 3.7 | 58.5 | 1.7
4.28 | 3.7 | 58.14 | 2.6
5.5 | 3.6 | 57.94 | 3.37
6.69 | 3.6 | 57.78 | 4.14
9.11 | 3.6 | 57.6 | 5.77
11.92 | 3.6 | 57.4 | 7.77
15.58 | 3.7 | 57.44 | 10.6
Conditions
Beam  4 keV
S. Yatom, N. Chopra, S. Kondeti, S. Walton, Y. Raitses

## Slide 41
N2 (%) | I(mA) | P_Ar (mTorr) | P_N2 (mTorr)
0 | 1.2 | 25 | 0
6.6 | 1.2 | 24.23 | 1.6
15.5 | 1.5 | 23.45 | 3.63
Changing Ar* Metastable Density with N2 at P ~ constant
P=25 mTorr , B=150 G
Conditions
S. Yatom, N. Chopra, S. Kondeti, S. Walton, Y. Raitses

## Slide 42
Effect of N2 Addition on EEDF
Langmuir probe measurements at PCRF & comparison with NRL results
EEDFs measured at the e-beam center.
Similar to previous measurements* by NRL
Consistent with a 0-D kinetic model:**
  Reduction ~2-5eV electron population due to inelastic electron energy loss to rotovibrational modes of the N2
Indirect evidence that the N2 addition also reduces also electron population responsible for the production of Ar*
Probe could not resolve energies   7 eV relevant to Ar 1sp5, 11.55 eV
Future work– deploy electron energy analyzer to measure  ~ 10’s-1000 eV
*D. Boris et al., Plasma Sources Sci. Technol. 22, 065004 (2013)
**G. M. Petrov et al., Plasma Sources Sci. Technol. 22, 065005 (2013)
Notes: 42

## Slide 43
Required CHT voltage to satisfy Isp requirements
Example:
Satellite diam. 0.8 m and length: 1 m
Altitude: 170 km
E-beams: 0.2 and 1 keV
From ion energy conservation:
Notes: 43

## Slide 44
Required (minimal) plasma density
From propellant utilization :
Underestimated minimal ionization degree required to generate the required thrust:
~ 10-20%
An initial target for experiment!
Notes: 44

## Slide 45: Advanced Confocal Laser Diagnostics for Industrial Reactors
A strong need in spatially and temporally resolved plasma diagnostics suitable for real industrial processing reactors
Limited diagnostic access on industrial reactors due to complex geometry, uniformity perturbation, and harsh environments
PPPL approach - an advanced confocal laser diagnostic using structured light laser beam
Successful implementation of Doppler-shift LIF on plasma source for industrial application
PPPL setup and diagnostics for studies of the industrial plasma source for ion implantation
Spatial resolution
PPPL LIF setup
Confocal (via 1 cm) vs Conventional IEDFs
I. Romadanov and Y. Raitses, Rev. Sci. Instrum. 97, 073002 (2023)

## Slide 46
TALIF: Absolute Density Measurements of H atoms in e-Beam Plasma
Larger Hydrogen density with B- field explains larger hydrogen coverage of graphene
Arthur Dogariu
Fs-TALIF
Broadband two-photon excitation:
  - Very efficient (high intensity in fs)
  - Low energy (10-100 J)
  Fast excitation (no quenching)
  Repeation: 1 kHz
H pump at 205 nm, record at 656 nm
Calibration: Kr pump at 204.1 nm, image at 826.3 nm

## Slide 47
Application example:
  Control of bandgap of 2D nanomaterials
  Graphene is zero bandgap semiconductor
  Fully hydrogenated graphene becomes wide bandgap material (5.4 eV) – important for emerging electronics
  ExB- plasma allowed to achieve a record high hydrogen coverage (36%) without damaging graphene
XPS results, ex-situ
Graphene hydrogenation in Ar+20% H2 ExB plasma
Fang, Raitses, Tully, Carbon 177 (2021)
Effect of the graphene exposure to EB plasma
D
G
D’
2D

## Slide 49
Effects of the gas pressure and the magnetic field on spoke
Xenon
Spoke disappears with the pressure depending on the magnetic field and the gas
Notes: 49

## Slide 50
Effect of the gas pressure is consistent with Simon Hoh instability
At low pressure (r) supports rigid rotor E×B ~ const
No visible spoke at high pressure, when E-field -> 0*
Xenon, Vd= 55 V, B= 50 Gauss
The same discharge current, 1.2 A
Ne
Te

  *Recall: neo  Er0 > 0
Notes: 50

## Slide 51
Gas pressure ~ 10-1 mtorr
Neutral density ~ 1012-1013 cm3
Plasma density ~ 1011-1012 cm-3
Highly ionized flow: ion/n > 100%
Ionization degree: from 10% to << 1%
Electron temperature ~ 20-100 eV
Ion temperature ~ 1 eV
Ion kinetic energy ~ 102-103 eV
Collisionless, partially ionized, non-equilibrium plasma with magnetized electrons and non-magnetized ions in highly non-uniform E×B fields, with strong pressure gradients
Hall thruster
Kraus and Raitses, Phys. Plasmas 25 (2018)

## Slide 52
Consider an ideal Hall thruster with only acceleration of single charge ions without cross-field electron transport, pressure gradients, plasma flow divergence ….
Hall current, , in the azimuthal direction is generated by the externally applied fields.
Hall current induces the magnetic field, .
From electromagnetic thrust (Ref *), the thrust density due to the magnetic force:
Theoretical thrust density limit for Hall thrusters
Electron Hall current,
Induced B-field,
External B-field,
Applied E-field,
*J. Simmonds, Y. Raitses, and A. Smolyakov, J. Electric Propulsion 2, 12 (2023)
For probably maximum thrust density for Hall acceleration

## Slide 53
Thrust density limits: theoretical vs achieved
Electromagnetic thruster limit
Hall thruster limit
Electrostatic thruster limit
Gridded ion thruster limit
For theoretical limits, assumed:
For FRC, MPD,
For Hall thrusters, (magnetic core material saturation)
For ion thruster,
NASA-457, theoretical for B=200 Gauss
*J. Simmonds, Y. Raitses, and A. Smolyakov, J. Electric Propulsion 2, 12 (2023)

## Slide 54
What if we would build HT to operate at limit?
Soulas et al. (2012)
Potential limitations:
  Excessive thermal heating of the thruster (e.g. anode by electron heat flux)
  Power losses due to enhanced electron cross-field transport
  Wall erosion
  Transition to MPD acceleration-?
Water/propellant cooling
Anode material
Pulsed operation
Short/Pulsed operation

## Slide 55
Anomalous electron cross-field transport
Spoke frequency ~ 10 kHz
10’s times slower than E/B
Conduct > 50-70% of the discharge current
Attributed to gradient drift instability (collisionless Simon-Hoh- type)
Large scale plasma structures
ExB rotating spoke in a Hall thruster
Small scale fluctuations
Plasma density oscillations and possible inverse energy cascade
Ellison, Raitses, Fisch, Phys. Plasmas 19 (2012)
Smolyakov et al., Plasma Phys. Control. Fusion 59 (2017)
Tyushev et al., Phys. Plasmas 30 (2023)
Wall-induced effect
in a 2 kW Hall thruster
Brown and Jorns, Phys. Rev. Lett. 130 (2023)
Raitses, Kaganovich et al., IEEE TPS 39 (2011)

## Slide 56
r
z
E
e-flow
Linear device with convenient diagnostic acess
DC-RF cathode or thermionic cathode to source non-thermal electrons with energies and fluxes comparable to Hall thrusters (~ A/cm2).
Flexible magnetic field to implement B-topologies relevant to Hall thruster and magnetic nozzle
Wall materials – for short circuity and SEE-induced near wall conductivity
10”- 6-way cross chamber
-Xe, Ar, Ar+H2, Ar+N2, Ar+CF4
-0.1-10 mtorr
-B-field,  103 Gauss
-RF power: 50-100W
-DC: 30-100 V, 1-3 A
e-Beam generated Penning discharge as a reference cell to study anomalous transport relevant to ExB thrusters
Raitses, Hendryx, Fisch, IEPC-2009-024 (2009)
Dielectric or conductive (biased or floating) wall

## Slide 57
Device\Parameter | R cm | L cm | T eV | B Gauss | Emax V/cm
E-beam ExB systems (PPPL, NRL, AMAT) | ~10-20 | ~50 | 0.1-10 | 100 | 1-2
LAPD at UCLA | 50 | 1700 | 2-5 | 400 | 4-18
Compact Auburn Torsatron | 17 | 53 | 10 | 1000 | 5
Blaamann | 8 | 65 | 9 | 570 | 2-6
Continuous Current Tokamak | 40 | 150 | 150 | 3000 | 120
ALEXIS at Univ. Auburn | 10 | 170 | 5 | 100 | 2
Reflex arc | 2.5 | 300 | 5 | 4000 | 20
Mistral | 11.5 | 140 | 1.4 | 220 | 
Maryland Centrifugal Experiment (MCX) | 27 | 250 | 3 | 2000 | 
WVU Q-machine | 4 | 300 | 0.2 | 1400 | 14
Hall thrusters | 2 | 2 | 20-100 | 100-300 | 500-1000
No linear device and other ExB systems can generate DC E-field comparable to Hall thrusters
Notes: Of all ExB devices using DC plasmas, the strongest electric field is realized in Hall thrusters – you can see that it can 2-3 orders of magnitude higher than different linear plasma devices and even tokamak

## Slide 58
Collisionless, partially ionized, non-equilibrium plasma with magnetized electrons and non-magnetized ions in highly non-uniform E×B fields, with strong pressure gradients
Hall thruster