## Slide 1: Plasma facing surface materials and their affects on LP pulsed plasma characteristics
Joel Brandon, Dr. Steve Shannon

## Slide 2: Summary
Summary
Background on topic
  Electron sources
  Secondary emission
  Dissociative recombination
Hypothesis
HPEM Modeling results
  Changes in [O] density
Chamber Setup
Experimental work
Future work
  Measurables
  Modifications

## Slide 3: Summary

## Slide 4: Electron Sources
Secondary surface electrons
  Photoelectric
    Photons
  Potential Ejection
    Ions
    Metastables
  Kinetic Ejection
    Fast Ions
    Fast neutrals
Ionizing collisions
  Electron – neutral
  Charge exchange
  Penning Ionization
  Associative detachment
Assumed
negligible
Dominant

## Slide 5: Potential Ejection - Auger Emission
Auger De-excitation
  2 possible pathways
“Theory of Auger ejection of electrons by metals” - Hagstrum 1954
Auger Neutralization

## Slide 6
2) Zaka-ul-Islam
OES of 844 O line emission in 300 mTorr plasma
-like mode separates E and H mode
  E-H transition supported by secondary electron emission

## Slide 7
LP measurements in CCP show change in EEDF through transition
Expect to see this change in and
5) Godyak 1992

## Slide 8: Modeling Efforts – recombination
3) Shibata et al
  As increases [O] decreases and [] increases
  As the O atoms available for dissociative recombination decrease, would increase, would decrease due to this equation

## Slide 9: Hypothesis
Through material considerations in source design we can create a new knob for transient control and power efficiency of pulsed plasmas by manipulating electron sources.

## Slide 10: Modeling

## Slide 11: Modeling - continued HPEM
Noticeable differences in [O] density at electrode
Unrecognizable difference in electron density

## Slide 12: Chamber Setup

## Slide 13: Chamber setup

## Slide 14: Review of experimental work

## Slide 15: Exp Design
Feedthrough on vacuum chamber allows rotation, effectively changing surface material of grounded cathode in active plasma
  No venting of chamber
6” diameter
One whole face covered in copper tape while one side remains aluminum

## Slide 16: Pulsing data for O2 on Cu and Al surfaces
SS density has changed
Visible difference in rate of rise at the point of E-H transition
Upon just flipping from Al to Cu, pressure reading changed by 3-4mTorr
  Possibly gas heating, dissociation, or ionization
Process was done with constant match settings
Readings on surfaces were alternated; Al, Cu, Al, Cu, Al, Cu
Data taken with LP
500Hz, 200W, 190 mTorr

## Slide 17: Smith Chart from surface to surface
Z=48.699 Z=51.026
4m

## Slide 18: E-H Transition
Current from VI probe plugged into O-Scope
Current decreases faster for aluminum, showing swifter transition from E-H mode
  Al surfaced plasma has more collisions resulting in higher plasma conductivity
It was hypothesized that this would exist as a result of changing the secondary electron emission coefficient by changing surface material
  Still undetermined if this is an effect of recombination or surface electron emission
Differences in re-matching vs constant match were minimal and showed same trend
E-H transition
Al Cu

## Slide 19: Electrode setup
Similar electrode setup to previous experiment
Surfaces are now thin film deposits
Surfaces tested
  Magnesium
  Aluminum
  Copper
  Silver`
Half wafer

## Slide 20: 50mT pulsed density
~30% increase in for silver surface
Opposite what would be expected from recombination effects

## Slide 21: 50mT EEDFs
Evolution of EEDF from transient to SS
High energy electrons play role in transient
High energy electrons lose their role with the silver cathode

## Slide 22: 100mT

## Slide 23: 100mT EEDFs
Still a similar evolution from 50mTorr but less difference between the 2 approaching SS

## Slide 24: 250 mTorr data
Less distinct temporal evolution as suggested by 50 →100 mTorr case
Longer term pulse to pulse change for Ag

## Slide 25: Early runs with silver thin film
Subsequent runs for material ~2 min apart
50mTorr Al outlier was last run
100mTorr Al outlier was 3rd of 5 runs

## Slide 26
Mesh netting to eliminate edge light-up
Degradation of silver coating after O2 plasma exposure
Degradation of copper film after O2 plasma exposure

## Slide 27: Future modifications to experiment

## Slide 28: Optical parametric oscillator for O atom measurements
(attachment for OPO)
Laser output 410-2500nm (18.5k) or 192-2750nm (62.7k)

## Slide 29: Future modifications
Expandable bellows for Langmuir probe insertion
Shrink chamber size
OES measurements for OH contamination
Re-oxidize surfaces when Al EEDF changes form
Compare machined Al surface with Al tape surface
  Surface roughness

## Slide 30: Review
Machined surface vs copper tape showed consistent changes in pulse profile as well as pressure change between the two surfaces
Differences in EEDF between surfaces stronger at low pressures
Visible difference in pulse density profile for recombination experiments
No visible difference in pulse profile for surface electron experiments
Silver degradation visible through first set of runs

## Slide 31: References
“Cold-cathode discharges and breakdown in argon: surface and gas phase production of secondary electrons” – Phelps and Petrovic 1999
“Energetic electron avalanches and mode transitions in planar inductively coupled radio-frequency driven plasmas operated in oxygen” – Zaka-ul-Islam 2011
“Effect of Surface Material on Spatiotemporal Structure in RF Glow Discharge” – Shibata et al 1995
“ adsorption on Silicon and Germanium” – Hagstrum 1961
“Evolution of the Electron-Energy-Distribution Function during rf Discharge Transition to the high voltage mode” – Godyak 1992
“Vacuum Thermionic Work Functions of Polycrystaliline Be, Ti, Cr, Fe, Ni, Cu, Pt, and 304 SS” –Wilson 1966
“Material dependent modeling of secondary electron emission coefficients and its effects on PIC-MCC simulation results of capacitive RF plasmas” – Daksha et al. 2019
“Recombination of neutral oxygen atoms on stainless steel surface” Mozetic and Zalar 2000