## Slide 1: Plasma Electrolytic Oxidation (PEO) at High Frequencies: Characterization and Control
IOPS Presentation: Patrick Hermanns

## Slide 2: Plasma Electrolytic Oxidation
Plasma (enhanced) Anodization
Al  Al2O3
Source: keronite.com

## Slide 3: Electrochemical process
OH-
H+

## Slide 4: Time dependent process

## Slide 5: Time dependent process

## Slide 6: Time dependent process

## Slide 7: Time dependent process

## Slide 8: Time dependent process

## Slide 10: Porous surface
Aluminum oxide melts and resolidifies on the surface
Crater-like structures at center of microdischarge ignition
Highly porous surface is established during coating
Problem: Microdischarge energy increases with time and locally destroys the oxide coating

## Slide 11: Problem
Electrical parameters
- Current amplitude I
- Pulse On-time Ton
- Pulse Off-time Toff
- Duty-Cycle
- Pulsing frequency f
Microdischarge behaviour
- Number density nMD
- Microdischarge size AMD
- Photo Intensity IMD
- Time constants
- Lifetme
- Electron density ne
Anode
t
I(t)
Ton
Toff
T = 1/f
?
I
nMD
, AMD , ne
,

## Slide 12: Experimental Setup
Electrolyte: dest. water + KOH
Anode material: Al 6061 alloy ()
Cathode material: stainless steel ()
Generator: Magpuls MP2-30, galvanostatic mode, unipolar (rectangular) pulsing

## Slide 13: MD Detection
Image analysis during process
Fast algorithm to enable in situ measurements
Threshold filter regarding photo-intensity to create binary image
MD size, number density and photointensity are calculated
Time for processing of one image:

## Slide 14: Parameter variation
Standard parameters:
Standard parameters:
Frequency
Current
Duty-Cycle

## Slide 15: Parameter variation
Standard parameters:
MD size and MD density can be controlled by changing the duty-cycle and the current density!
Frequency
Current
Duty-Cycle

## Slide 16: Lifetime of MDs (current pulses)

## Slide 17: Lifetime of MDs
Analysis of current pulses by wavelet transform
Fitting of wavelet function by translation b and dilation s:
Wavelet coefficients (like fourier coefficients):
Source: towardsdatascience.com

## Slide 18: Results wavelet transformation
Lifetime of MDs is in the kHz range! Influence of frequency in this region?

## Slide 19: Phase resolved MD dynamics
f = 5 kHz
f = 100 kHz
MDs cannot follow the generator frequency if the pulsing time is shorter than the MD lifetime!

## Slide 20: In situ MD control scheme

## Slide 21: Results MD control (camera)
MD size
MD number

## Slide 22: Results MD control (pictures)
Uncontrolled
Controlled

## Slide 23: Results MD control (OES)
Uncontrolled

## Slide 24: Results MD control (OES)
Controlled

## Slide 25: Results MD control (SEM)
Uncontrolled
Controlled

## Slide 26: Conclusion
MD lifetime is in the range between 6 µs and 1600 µs
Current density and duty-cycle can adjust the MD number density and size
Pulsing frequency has to be in the range of the microdischarge lifetime to control microdischarges
Microdischarge properties can be controlled to distinct values with an in situ closed-control loop. By this the microdischarge energy can be controlled indirectly
Outlook: Further material characterization of produced oxide coatings

## Slide 27: Thank you for your attention! Special thanks to people from:
1Hermanns et al. 2020 J. Phys. D: Appl. Phys. 53 435204
2Hermanns et al. 2021 J. Phys. D: Appl. Phys. 54 045205