## Slide 1: Pulsed plasma for plasma processing
Steven Shannon
Presented at the Online LTP Seminar
26 May 2020
Work shown has been supported by The National Science Foundation, Samsung Electronics, Applied Materials, and MKS Instruments

## Slide 2: Plasma Science at NCSU
Emphasis is on industrial and medical applications as well as fusion science
Four faculty
  Mohamed Bourham – fusion science, plasma assisted coatings, plasma material interactions
  Katharina Stapelmann – biological and medical applications
  Alexander Bataller – ultrafast spectroscopy, laser plasmas
  Steve Shannon – industrial applications, fusion science, advanced diagnostics, RF systems
13 graduate student researchers, 4 undergraduate researchers

## Slide 3: Plasma Science is one of the NE focus areas
Power design and safety analysis
Security and non-proliferation
Plasma science and engineering
Materials, waste forms, and storage
Computational science
Radiation science and engineering
133 undergrads, 123 graduates, 22 faculty, 2 centers (CASL and CNEC), and 1 nuclear reactor
$9.5 million in research expenditures and 17 new grants awarded in FY2016

## Slide 4: All I have to do is talk…
Joel Brandon
Yao Du
Kristopher Ford
Elijah Martin
John McDuffie
David Peterson
Carl Smith
Matthew Talley
Yuhua Xiao
Abdullah Zafar
Plus countless collaborators, co-workers, and other students – Naman Bhatt, Cade Binkley, Brandon Byrns, John Caughman, Lee Chen, Thai Cheng Chua, Hamilton Clark, David Coumou, Corey DeChant, Vincent Donnelly, Ahmed El-Saghir, Valery Godyak, David Graves, David Green, Casey Icenhour, Brayden Myers, Kyung Sun Kim, Travis Koh, Philip Kraus, Theresa Kummerer, Mark Kushner, Alex Lindsay, Richard Martineau, Ervin Miller, Josh Morsell, Sang Ki Nam, Alok Ranjan, Katharina Stapelmann, Mohammed Shutafyi, Shaun Smith, Peter Ventzek, John Verboncour, Russ Westerman, Scott White, Jang-Gyoo Yang, Yiting Zhang

## Slide 5: Overview of presentation
Pulsed plasmas for manufacturing – a brief introduction
Power coupling into pulsed systems
Time resolved diagnostics for pulsed systems
Electronegative plasmas in pulsed environments
Closing remarks

## Slide 6: Why Pulsed Plasmas
Steady state conditions are governed primarily by particle and energy balance
Forcing transient conditions open up a wider range of temperatures (chemistry) and densities (flux)
Additionally, timing of chemistry and particle flux can be staged through phase lock pulsing
2D fluid model of 5 kHz pulsed ICP. 320 W, 20 mTorr Cl2[2]
D. Economou. Journal of Physics D: Applied Physics 47.30 (2014): 303001.
S. Banna et. al Journal of Vac. Sci. and Technol. A 30, 040801 (2012)

## Slide 7: Time varying plasmas present significant challenges for efficient RF power delivery in processing systems
Slow transients demand smooth impedance matching and power compensation – consistent tuning trajectories, accurate power measurement (gas transitions during short process steps (BARC open, endpoint of large open area processes, etc.)
Rapid transients (RF pulsing, Bosch, magnet pulsing, step transition) do not have manufacturing-ready auto tuning match solutions (but there are some really good ideas out there). Matching network and antenna design need to account for transient impedance mismatch during specification and design
This talk will introduce these problems and present some examples on how they may be addressed
13.56 MHz
50% D.C.
1kHz Pulse
200W Peak
Ground
Electrode
RFEA

## Slide 8: A motivational illustration
Assumes a 1010cm-3 Ar plasma with 100V bias on bottom electrode
Passive L-type match with typical series and shunt circuit elements
Significant power transients generated due to Vbias dependence on ne as well as load impedance shift due to pulse cycle.
Within-pulse measurement and control loop response is needed to stabilize these systems over larger process ranges

## Slide 9: The basic challenge – control for complex features
Harmeet Singh, “Overcoming challenges in 3D NAND volume manufacturing, Solid State Technology Magazine, July 2017
Dick James, “The Second Shoe Drops – Samsung V-NAND Flash”, www.chipworks.com, 5 August 2014
Control of ions and reactive species are critical for the formation of complex features (such as HAR and atomic layer processes). Partitioning power between these key parameters is a key step in plasma source optimization for manufacturing.

## Slide 10: What are we trying to optimize (and trying to avoid)?
What we want
Uniform power deposition (or power based uniformity control)
Controllable deposition in plasma and sheath regions
Reproducible power WTW and in single processes
Fast time response
What we don’t want
Unreasonable power mismatch
High dissipation in non-plasma elements
Narrow operating range and control levels
Unnecessary power delivery complexity
These are by no means exhaustive lists of what we want and what we don’t want. These are only examples taken from a larger list to motivate topics in this presentation

## Slide 11: Pulsed ICP power delivery
VI Probe
VI Probe
Langmuir
Probe
Inficon Triple gauge
Baratron gauge
Throttle
Valve
Turbo Pump
Gas Inlet
Directional coupler to Network Analyzer
RF in
Foreline
Gas Out
Optical Window
Capacitance Controls
Foreline gauge
20 – 290pf
3.5 turn copper coil
Symmetrical chamber gas flow
Pre-match impedance measurement
50mTorr Baratron gauge

## Slide 12: Transient measurements – high resolution time measurements for pulsed RF systems

## Slide 13: How do we measure density on sub microsecond time scales?
Resonator
Loop Antenna
Coaxial Cable
Metal Ring
Insulating Ring
Ground
Resonator
DC Float
Resonator

## Slide 14: Collisional and Sheath Considerations
l
w
Simplified Probe/Plasma
Model
l
w
Collisional Model
l
Sheath Model
w
Wire radius = a
Sheath thickness = b
Sands et. al. PSST 16 (2007) 716-725

## Slide 15: Pulsed ICP power delivery
VI Probe
20 – 290pf
3.5 turn copper coil
Symmetrical chamber gas flow
Pre-match impedance measurement
50mTorr Baratron gauge

## Slide 16: What can we use an integrated plasma / match model for?
Chart: Best Matched Frequency 350pf
| 1010000000 | 5000000000 | 8000000000 | 10000000000 | 50000000000 | 80000000000
Frequency | 13.025 | 13.05 | 13.05 | 13.05 | 13.3 | 13.5
Frq Tuned Delivered Power Ratio | 0.27273 | 0.52941 | 0.58333 | 0.61165 | 0.96154 | 0.97403 | 1
13.56 Delivered Power Ratio | 0.11111 | 0.14141 | 0.17874 | 0.2 | 0.80488 | 0.93258 | 1
Chart: Best Matched Frequency 100pf
| 1010000000 | 5000000000 | 8000000000 | 10000000000 | 50000000000 | 80000000000
Frequency | 13.2 | 13.2 | 13.2 | 13.2 | 13.4 | 13.5
Delivered Power | 0.6 | 0.8 | 0.83333 | 0.87179 | 1 | 0.97701
13.56 Delivered Power Ratio | 0.2 | 0.24138 | 0.28947 | 0.29268 | 0.82609 | 0.91071 | 0.86111

## Slide 17: This could enable tailored power delivery
Chart: Transient Matching @ 12.5mTorr
13.3
13.35
13.4
13.5
13.525

## Slide 18: Simplified ICP model for circuit analysis
Power Supply
Power Conditioning
Hz
Eq
L11
L12
L22
Rp
Lp
Rp and Lp contain plasma parameters – ne (same as capacitive model), neff and seff (collisional terms with stochastic modifications), and dp (skin depth, depends on ne, collision terms, and Te). If we have a good collision model we can build a similar impedance matrix for ne and Te here

## Slide 19: Combining plasma model with chamber design
L11
L12
L22
Rp
Lp
13.56 MHz
Plasma load
Inductive Antenna
Antenna termination
Matching Network
VI Probe
20-290pF
20-290pF
700 nH
N=3.5 Rcoil=2.1”
Lcoil = 4”
100-500pF
Rplasma = 2”
Lplasma = 6”

## Slide 20: Plasma parameters vs. electrical impedance
1 eV
2 eV
3 eV
4 eV
5 eV
1 x 1011 cm-3
3 x 1010 cm-3
1 x 109 cm-3
1 x 1010 cm-3
3 x 109 cm-3
1 eV
2 eV
3 eV
4 eV
5 eV
1 x 109 cm-3
3 x 109 cm-3
1 x 1010 cm-3
1 x 1011 cm-3
3 x 1010 cm-3
5 mTorr Argon
50 mTorr Argon
Good variability of load impedance with respect to density and temperature give a non-invasive method to measure key plasma parameters for process development and studying new source configurations

## Slide 21
How Accurate is the Model? Always an important question to ask
Chart: Pressure p (mTorr)
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50
Ne | 99174900000000000 | 1.321e+17 | 1.7533e+17 | 2.0874e+17 | 1.9249e+17 | 2.1356e+17 | 2.2061e+17 | 2.6162e+17 | 2.4111e+17 | 2.6497e+17
Calculated Ni | 74045086637585984 | 92354311108948560 | 1.3897e+17 | 1.7153e+17 | 2.1381e+17 | 2.5654e+17 | 3.0537e+17 | 3.3784e+17 | 3.72e+17 | 4.0226e+17
Comparison of ne calculated () from circuit equations with measured ne taken with a Langmuir probe ()
Ar, 75W applied RF at 13.56MHz
ICAROS Reactor, NCSU

## Slide 22: Typical Global ICP Model (Leiberman)
L11
L12
L22
Rp
Lp
RF
Plasma load
Inductive Antenna
Antenna termination
Matching Network
VI Probe
This assumes a “thin skin depth” approximation for the transformer equations. Skin depth is only accounted for in plasma resistance and plasma inductance.
Does skin depth impact transformer coupling parameters? (Spoiler… it does)

## Slide 23: Overall Impact of a Circuit Model
Integrated plasma / circuit model does a good job capturing most trends, but power on density trajectories have never quite matched up as well.

## Slide 24: Impact of Skin Depth Dependence
When λR  0 radial current density profile converges to solution of a solenoid
Paramount to capture impact that skin depth has on evolution of plasma parameters in ON-Cycle
  Lieberman’s equivalent circuit model of a plasma assumes a thin skin depth for all relevant components
  Distribution of current is at the edge of the plasma

## Slide 25: Impact on L12 & L22

## Slide 26: Dependence on Plasma Radius (RPlasma)

## Slide 27: Still missing that “concave up” feature
Maxwellian EEDF
Druyvesteyn EEDF
Generalized EEDF
Seo et al, Journal of the KPS 48(3) 414-421 (2006)

## Slide 28: The Generalized EEDF
The evolution of the EEDF from a Druyvesteyn in the early on cycle to the Maxwellian at close to SS can be captured via a generalized EEDF
Where
*Note: Γ is the incomplete lower gamma function

## Slide 29: What does this look like?
Some Notes:
Reduced Ionization efficiency when g>1
dne/dt converges for all cases when g=1
ne Lower Bound occurs at starting density
ne Upper Bound occurs at inflection point
Pressure dependence is expected as dne/dt rises with decreasing pressure

## Slide 30: What happens if we keep g constant?
Dne/dt and ionization decreases g2. This is responsible for concavity

## Slide 31: Possible source of concavity change
Constant EEDF
Modulating EEDF
-Concavity is caused by an upward shift in the high energy tail of the EEDF.
-The increase in the rates of ionization, excitation and elastic scattering cause an inflection point.

## Slide 32: High Energy Tail
Tail at early on cycle
Tail at steady state
Depressed ionization at early on cycle characteristic of upward concavity

## Slide 33: Takeaways

## Slide 34: What about chemistry control in pulsed systems
Consider idealized case of [X](t)
An RF pulse of long duration creates a pseudo-steady state
At discrete times in the afterglow, shine a light for data points related to [X]
Plot those data points as an exponential decay to find kTotal
RF trigger pulse
Free radical density
Ideal snapshot in time → kTotal
t
Active Glow
After Glow
Laser
Laser Induced Fluorescence (+) and Pulse Induced Fluorescence (o) results for CF2 in CF4 capacitively coupled plasma[1]
[1] - Hancock, G. et al. Journal of Physical Chemistry 94.8 (1990): 3269-3272.
Laser

## Slide 35: Pulse Induced Fluorescence Method
Vary the off time between active RF pulses of 10 ms (to reach same steady state regardless of off time)
Collect radical emission, which is proportional to [X]
Normalize it to long on time, steady state intensity [X]0 and find kTotal
toff,1
toff,2
RF trigger pulse
Free radical density
Ideal snapshot in time → kTotal
t
t
t
[1] - Hancock, G. et al. Journal of Physical Chemistry 94.8 (1990): 3269-3272.
PIF raw data in CF4 capacitively coupled plasma[3]
Active Glow
After Glow
Spectrometer

## Slide 36: What can we get from PIF?
[1] Gibson et al. Plasma Phys. Control. Fusion 59 (2017)
Top - HPEM Density profiles at radial and axial center of processing ICP. Bottom – Radical:Ion Flux Ratio at Wafer Surface[1]
O2 plasma generates atomic O
In plasma afterglow, [O] decay comes from pumping and surface loss
ktotal is measured through study of intensity decay of atomic O. From diffusion theory
– total surface loss probability is final result
 - surface recombination to form O2 is result if experiment is known to exclude other reactions
– Characteristic diffusion length
– O/O2 Diffusion coefficient
– Thermal Velocity
V/S – Volume to surface ratio

## Slide 37: PIF Challenges
Temperature poses a challenge, on multiple levels (GEC 2018)
1 – Tw varies with average power
2 – Tg is assumed for final calculation (+/- 50% or more error)
3 – Tg varies within the pulse and so total gas density varies
Clearly need a way to quantify temperature
– Characteristic diffusion length
– O/O2 Diffusion coefficient
– Thermal Velocity
V/S – Volume to surface ratio
toff,1
toff,2
t
t
Tg
Tg
t
Tg

## Slide 38: Improving PIF – Tg(t) from Trot(t)
Figure 2[1]. Flow chart for determining if N2(C3Πu v’=0 → B3 Πg v’’=0) is in equilibrium with translational temperature of Cl2
Measured Trot of the molecular gas
N2 emission is brighter, more easily characterized than O2 rotational bands (2nd positive system in 334 nm band)
Tg reduces the uncertainty in D, vth of β expression
Tg corrects emission intensity as well
[1] Q. Wang et al. 2007 J. Phys. D: Appl. Phys. 40 4202
[2] T. Ma et al. J. Appl. Phys. 125, 023301 (2019);
High Pressure Case
N2(Tr=Tg) + *M / e- → *N2(Tg≠Tr) + *M / e-
*N2(Tg≠Tr) + X(Tr=Tg) → → *N2(Tr=Tg) + X(Tr=Tg)
*N2(Tr=Tg) → N2(Tr=Tg) + hv(Tr)
Low Pressure Case
N2(Tr=Tg) + e- → *N2(Tr=Tg) + e-
*N2(Tr=Tg) → N2 + hv(Tr)
Figure 3[2]. Gas temperature from Trot of N2 in a Cl2/O2 plasma

## Slide 39: Rotational Spectra
Trial Tr are used to calculate full spectrum and the best fit determined from χ2 error minimization
MATLAB code is available in dissertation
Key criterion – uncertainty in Tr (is our sharpening tool too coarse?)
Pure simulation lines for J=40

## Slide 40: Time Resolved Tr
Quantified experimental error through replicates
Quantified simulation error through bootstrap method

## Slide 41: Tr(t) Results
Plasma conditions: 200 W, 50 mTorr, 95/5% O2/N2
Pulsed with 10 ms main pulse, 1 ms probing pulse with 12.5 Hz frequency
Tr relative error was between 6-9% for all cases
Heating and cooling rates were remarkably close (85%)
Used fits to generate Tg(t) correction for PIF, which had a higher sample rate
Time resolved temperature results after main pulse
Example spectrum with simulation fit

## Slide 42: Improving PIF – Experiment
Confined plasma region isolates atomic O loss on quartz
Probing pulse fixes Twall
Echelle provides data for Tr(t), PI-Max provides I(t) data for β
200 W, 50 mTorr with 95/5% O2/N2 chosen for higher signal-noise ratio
Wavelength filter isolates 844 nm line of O
Gas Delivery
Aspheric Lens
Matching Network
Triple Gauge
Baratron
Roughing Valve
Directional Coupler
13.56 MHz Generator
Off-Axis Parabolic Mirror
Pinhole Aperture
Aspheric Lens
Wavelength Filter
PI-Max3 iCCD
Gas Outlet
Echelle 4000+ Spectrometer
Fiber
External Trigger

## Slide 43: Improved PIF Data
Applied temperature correction to account for changing gas density
  Ideal Gas Law
i refers to discrete data in the afterglow, ss to the steady state values
The starting intensity is what we care about – must necessarily be lower and so ktotal will increase
Example 10 µs acquisition from iCCD
Example temperature correction for one pixel, one probe pulse

## Slide 44: PIF Data processing
Project main pulse backwards, Obtain Idiss exc
Azimuthally Average
Multiply each I(t) pixel by Tr(t) fit
Subtract Idiss exc pixel by pixel
Normalize Ring Data
Find I(toff) at each ring
Fit 2 exponential decay
Use k constants to calculate β
~5 GB of iCCD data
[1] - Cartry, G., L. Magne, and G. Cernogora 2000
Decay data for outermost ring

## Slide 45: Results
Two decay coefficients for ktotal,1 and ktotal,2 leads to two loss coefficients
Immediate afterglow β1 is more applicable for plasma processing
Without Tg correction β1=[0.23,0.79] considering Tg assumption from [400,500] K and goodness of fit
β1 is higher than any literature value
  Pressure dependence, source type
GEC 2019
[10] – Gilles Cartry et al 2006 Plasma Sources Sci. Technol. 15 479
[14] - J P Booth et al 2019 Plasma Sources Sci. Technol. 28 055005
[24] - Fletcher, D. & Meyers, J. Journal of Thermophysics and Heat Transfer 31.2 (2016)
[96] - S. Wickramanayaka et al. Japanese journal of applied physics 30.11R (1991)

## Slide 46
2) Zaka-ul-Islam
OES of 844 O line emission in 300 mTorr plasma
-like mode separates E and H mode
  E-H transition supported by secondary electron emission

## Slide 47: Modeling Efforts – recombination
3) Shibata et al
  As increases [O] decreases and [] increases
  As the O atoms available for associative recombination decrease, would increase, would decrease due to this equation

## Slide 48: Modeling - continued HPEM
Noticeable differences in [O] density at electrode
Very small difference in electron density

## Slide 49: Pulsing data for O2 on Cu and Al surfaces
SS density has changed
Visible difference in rate of rise at the point of E-H transition
Upon just flipping from Al to Cu, pressure reading changed by 3-4mTorr
  Possibly gas heating, dissociation, or ionization
Process was done with constant match settings
Readings on surfaces were alternated; Al, Cu, Al, Cu, Al, Cu
Data taken with LP
500Hz, 200W, 190ish mTorr

## Slide 50: Enabled transient density study for pulsed RF as well as plasma oscillations

## Slide 51: Closing remarks
Plasmas operated outside of steady state conditions through repetitive pulsing present a wider range of operating conditions than can be achieved through steady state power dissipation
Tool design considerations ranging from power delivery, impedance matching, and material selection can influence these transient conditions
Simplified plasma models that enable integration with equivalent circuit models of plasma sources lend some insight into mechanisms that drive transient conditions
Time resolved plasma diagnostics further serve to validate these models and provide insight into how these sources respond to modulated power
Kevin Gibb, “Samsung’s 14 nm LPE
FinFET Transistors”, EETimes, 2016